# Simple strategies to enhance efficiency and stability of nano-film electrodes in solar energy conversion processes

Hikmat S. Hilal, An-Najah N. University, Nablus, Palestine

Ahed Zyoud, An-Najah N. University, Nablus, Palestine

### Abstract

Metal chalcogenide (MX; M = Cd, Cu, and others; X = S, Se or Te) polycrystalline film electrodes of are widely assessed in photoelectrochemical (PEC) solar energy conversions, for many reasons1.  These films are commonly prepared by chemical bath deposition, electro-deposition or other simple methods, but normally suffer low stability and low PEC conversion efficiency (<1%)2. Enhancement is being actively investigated3. According to US-DOE, maximum conversion efficiency for these electrodes in 2020 is expected to be ~15%.  To further enhance the electrode characteristics, we have use two simple strategies. Controlled film annealing and cooling rate is used to enhance particle characteristics (conductivity, interconnection, adherence, band gap value). Each metal chalcogenide film needs specific annealing temperature and cooling rate3-5. To enhance charge transfer across the solid/redox couple interface, electrodes were coated with electro-active materials inside polymeric films, where the electro-active materials behave as charge transfer catalysts. Faster hole transfer to redox couple occurs, which increases photocurrent density6. Hole accumulation in the space-charge-layer (responsible for electrode photo-corrosion) is also prevented. Such model is summarized in Figure 1.  By combining both strategies together, metal chalcogenide film electrode stability and efficiency have been remarkably enhanced here. High efficiency values (~12 -18%) have been observed here for metal chalcogenide films6-7. Details of results and their discussions will be described. Theoretical models will also be presented to explain how the modification methods affect both conversion efficiency and film stability. Future prospects of metal chalcogenide film electrodes will be critically discussed, in terms of economic feasibility, environmental impact and recyclability.

Recent Publications

- Tachan Z, Shalom M, Hod I, Ruhle S, Tirosh S, Zaban A, (2011) PbS as a highly catalytic counterelectrode for polysulﬁde-based quantum dot solar cells. Journal of Physical Chemistry C 115: 6162–6166.

- Emin S, Singh S.P, Han L, Satoh N, Islam A (2011) Colloidal quantum dot solar cells. Solar Energy 85: 1264–1282.

- Sabri H, Saleh S, Zyoud A, Saadeddin I, Campet G, Park D-H, Faroun M, Hilal HS (2014)  Enhancement of CdSe film electrode PEC characteristics by metalloporphyrin/polysiloxane matrices. Electrochimica Acta, 136: 138-145.

- Zyoud A, Murtada K, Kwon H, Choi H-J, Kim T-W, Helal M, Faroun M, Park D-H, Hilal HS (2018) Copper selenide film electrodes prepared by combined electrochemical/chemical bath depositions with high photo-electrochemical conversion efficiency and stability, (Solid State Sciences 75: 53-62.

- Zyoud A, Al-Yamani S, Bsharat H, Helal M, Kwon H, Park D-H, Hilal HS (2018) Recycled polycrystalline CdS film electrodes with enhanced photo-electrochemical characteristics. Materials Secience in Semiconductor Processing 74: 277-283.

- Zyoud A, Al-Kerm R, Al-Kerm R, Mansur W, Helal M, Park D-H, Sabli N, Hilal HS (2015) High PEC conversion efficiencies from CuSe film electrodes modified with metalloporphyrin/polyethylene matrices, Electrochimica Acta. 174: 472-47.

- Zyoud A, AlKerm R, Alkerm R, Abdelhadi D, Park D-H, Helal M, Campet G, Muthaffar R, Kwon H, Hilal HS (2016) Enhanced PEC characteristics of pre-annealed CuS film electrodes by metalloporphyrin/polymer matrices. Solar Energy Materials and Solar Cells 144: 429–437.

Figure 1: Charge transfer catalysis formalism at

solid/redox couple interface

Biography

Hikmat S. Hilal is a distinguished Professor of inorganic and materials chemistry, with a DSc degree. His research is focused on solar energy applications (photovoltaics and environmental cleanup) using enhanced semiconducting materials.  He established research groups in Palestine and published more than 100 articles in the area. He published 6 research books/book chapters and presented more than 150 invited talks in international conferences. He has been granted a number of awards for his achievements in photoelectrochemistry.

Email: hshilal@najah.edu

Notes/Comments: