NOTE: This research paper was sent to the 16th International Conference on Emerging Materials and Nanotechnology, Mar 22-23, 2018, London, UK., to presented (oral speaker), but the UK Government do not grant me a visa to attend the conference although I have pay the registration fee.

Title: “(PANI-PTSA) & CoFe2O4/Co0.5Zn0.5Fe2O4  - Nanocomposite Absorption Materials Prepared for EMI Shielding in Microwave X-band”.

Jameel M. A. Sulaiman1, 2*, Sewench N. Rafeeq1     Mukhils M Ismail1, Avinandan Mandal 3

1 Department of Applied Sciences, University of Technology, Baghdad, Iraq

2 College of Dentistry, University of Mosul, Mosul, Iraq

3 Key Lab of Rubber‑Plastics, Ministry of Education/Shandong Provincial Key Lab of Rubber‑Plastics, School of Polymer Science and Engineering, Qingdao University of Science and Technology, Qingdao 266042, China

Email: jmasulaiman@gmail.com

Keywords:

Nanocomposite, (Cobalt – Zinc) Ferrite, PANI-PTSA, EMI Shielding, Microwave X-band.

- Abstract

The risk of Electromagnetic Interference (EMI) waves is constantly required to materials work as shielding, which are widely used in various high technology applications such as medical, communications, military. Polyaniline (PANI-PTSA) & Ferromagnetic - Cobalt Ferrite {CoFe2O4}/Cobalt-Zinc ferrite {Co0.5Zn0.5Fe2O4} nanocomposites are one of these materials which are mix together to have found a solution for these problems.  Methodology & Theoretical Orientation: Polyaniline doped Para Toluen Sulfic Acid (PANI-PTSA) be set up by substance oxidative polymerization of aniline in aqueous medium with ammonium peroxydisulphate as an oxidant. The sol–gel auto combustion method has been used to synthesis ferrite samples. Nicholson–Ross–Weir (NRW) method was applied to determine the real and imaginary parts of complex relative permittivity (εr'-jεr'') and permeability (μr'-jμr'').Findings: The composite materials showed maximum absorption frequency range reflection loss of CFP was -7.1 dB at 9 GHz and -9.6 dB at 11.2 GHz, while at the same frequency for CZFP was -17.1 dB and -23.7 dB respectively. Conclusion & Significance: Result indicated that CZFP was the best (> 98% power absorption) than CFP (>50% power absorption).

- Image

- References

- Sewench N. Rafeeq, Mukhils M. Ismail, and Jameel M. A. Sulaiman, “Magnetic and Dielectric Properties of CoFe2O4 and CoxZn1-xFe2O4 Nanoparticles Synthesized Using Sol-Gel Method”, Journal of Magnetics 22(3), 406-413 (2017), ISSN (Print) 1226-1750, ISSN (Online) 2233-6656.

- Mukhils M Ismail, Sewench N. Rafeeq, Jameel M. A. Sulaiman, Avinandan Mandal, “Electromagnetic interference Shielding and Microwave Absorption Properties of Cobalt Ferrite CoFe2O4 / Polyaniline Composite”, Applied Physics A (2018) 124:380 https://doi.org/10.1007/s00339-018-1808-x

- Nasrin S, Manjura S, Hoque F. U. Chowdhury Z, and Moazzam M. Hossen, “Influence of Zn substitution on the structural and magnetic properties of Co1-xZnxFe2O4 nano-ferrites” J. Appl. Phys. (IOSR-JAP), 6, 58 (2014).

- Chung D.D.L, “Materials for electromagnetic interference shielding”. Journal of Materials Engineering and Performance, 2000. 9(3): p. 350-354.

- Wu J.H. and Chung D.D.L, “Combined use of magnetic and electrically conductive fillers in a polymer matrix for electromagnetic interference shielding”. Journal of Electronic Materials, 2008. 37(8): p. 1088-1094.

- Sanjeev Kumar, Vaishali Singh, Uttam K. Mandal, R.K. Kotnala”, Nanocrystalline Co0.5Zn0.5Fe2O4 ferrite: Synthesis, characterization and study of their magnetic behavior at different temperatures", Inorganica Chimica Acta, 2015, 428, 21-26.

- Gul I. H and Maqsood A, “Structural, magnetic and electrical properties of cobalt ferrites prepared by the sol–gel route” J. Alloys Compd. 227-231, 465 (2008).

- Gul H I, Abbasi A Z. Amin F, Anis-ur-Rehman M, and Maqsood L. H A, “Structural, magnetic and electrical properties of Co1-xZnxFe2O4 synthesized by co-precipitation method” J. Magn. Magn. Mater. 311, 494 (2007).

- Nicolson AM, Ross GF. Measurement of the intrinsic properties of materials by time-domain techniques. IEEE Trans. Instrum Measur. 1970; 19:377–382.

- Ratheesh R, and Viswanathan K, “Chemical Polymerization of Aniline Using Para-toluene Sulphonic Acid”, IOSR Journal of Applied Physics (IOSR-JAP) 2278-4861. Volume 6, Issue 1 Ver. II (Feb. 2014), PP 01-09.

- Biography

Full Name: Jameel Mohammed Ameen Sulaiman

Contact number: +9647701682891
Twitter account: @jameel_sulaiman
Linked In account: Jameel Sulaiman

Session name/ number: First
Category: (Oral presentation)

- Presenting author details

Jameel Sulaiman

B.Sc. Physics – 1982, University of Baghdad. M.Sc. Physics – 2005, University of Mosul. PhD; Applied Physics - 6/6/2018, Technology University, Baghdad.

He has built his expertise during years of hard work in R&D centers in Iraq since (1988-2003), then (2005) in evaluation, teaching and administration both in education institutions at University of Mosul College of Dentistry.

He has a number of applied researches and published locally and internationally. In addition to my participation in a number of local and international conferences in Turkey, Saudi Arabia, UAE … as well as a training course in Switzerland.