# Structural, Magnetic and Dielectric Properties of Sm3+ and Mn2+ Co-doped BiFeO3 Nanoparticles

Syed Irfan, PhD, Tsinghua University, Beijing China

Kiani M., Msc, National University of Science and Technology, Islamabad Pakistan

Syed Rizwan, PhD, National University of Science and Technology, Islamabad Pakistan

Abstract (300 word limit)

The structural, morphological, magnetic and dielectric properties of Samarium (Sm3+) and Manganese (Mn2+) doped Bismuth ferrite (BSFMO, Sm=5% and Mn=0%, 5%, 10%, 20%, 25%) nanoparticles are presented which were characterized by X-ray diffraction (XRD), scanning electron microscope (SEM), superconducting quantum interference device (SQUID) and LCR meter, respectively. The XRD and SEM measurement show that the nanoparticles were successfully synthesized by an improved sol-gel technique. The nanoparticles size decreases with increase in the Mn2+ concentration. The dielectric measurement revealed that the dielectric constant and dielectric loss decreases at higher frequency. The saturation magnetization and the magnetic coercivity of Mn-doped BSFO decrease by increasing Mn concentration which is attributed to the increase in Bi2Mn4O9 antiferromagnetic impurity phase and the increase in antiferromagnetic spin wavelength. Our results suggest that the resulting nano composite is a soft ferromagnetic material and is a suitable candidate for magnetic sensors operable at room-temperature. 
Image

Recent publications (minimum 5)

- Irfan S, Li L, Saleemi AS, Nan CW (2017) Enhanced photocatalytic activity of La3+ and Se4+ codoped bismuth ferrites nanostructures Journal of Material Chemistry A DOI: 10.1039/c7ta01847a.

- Irfan S, Rizwan S, Shen S, Li L, Asfandiyar, Butt S Nan CW, (2017) The Gadolinium (Gd3+) and (Sn4+) codoped BiFeO3 nanoparticles as new solar light active photocatalyst 7:42493-42505.

- Irfan S, Shen Y, Rizwan S, Wang HC, Khan SB, (2017) Band-gap engineering and enhanced photocatalytic activity of Sm and Mn doped BiFeO3 Journal of American Ceramics Society 100:31-40.

- Irfan S, Kiani M, Rizwan S, (2017) Structural, magnetic and dielectric properties of Sm3+ and Mn2+ co-doepd BiFeO3 nanoparticles Journal of powder metallurgy and mining 6: 1000163-1000167.

5.   Irfan S, Rizwan S, Shen Y,Tomovska R, Zulfiqar S, Zulfiqar MI, Nan CW (2016) Mesoporous template-free gyroid-like nanostructures based on La and Mn co-doped bismuth ferrites with improved photocatalytic activity RSC Advances 6:114183-114189.

Biography (150 word limit)

Syed Irfan Ali is a Senior PhD Scholar in Tsinghua University, Beijing China. He is currently working on purification of water by photocatalytic degradation of polluted organic compounds (colored and colorless). Currently, he is also working as a editorial board member in journal of powder metallurgy and mining and International journal of Material Science and Application. Also working as Reviewer in “Journal of Physics and Chemistry of Solids” and 2nd International Conference on Biological Sciences and Technology.

Email: irfansyed715@gmail.com

Contact no: 0086188131644552

Category: Oral

Notes/Comments: