Improvement Microstructure and Hot Corrosion Resistance of Plasma Sprayed Thermal Barrier Coatings by 20%wt Al2O3 Addition

Prof. Dr. Mohammed Jasim Kadhim,

Prof. Dr. Sami Abualnoun Ajeel,

Lect. Ali Mezher Resen

Department of Production Engineering and Metallurgy, University of Technology, Baghdad, Iraq.

### Abstract

This study aimed to study effect of alumina addition to yttria partially stabilized zirconia on microstructure and hot corrosion performance of  20%wt Al2O3 + YSZ composite thermal barrier coatings (TBCs) in the presence of molten eutectic mixture of Na2SO4 + V2O5 at 900 ◦C at different times are 1, 10, 40 and 80 Hrs. and comparison with conventional YSZ. The 20%wt Al2O3 + YSZ composite coatings are prepared by atmospheric plasma spray (APS). Upper surface plan views of the coatings are examined using scanning electron microscopy (SEM) to observe the morphological and microstructural changes. Element analysis and phases are identified for both conventional and composite. The hot corrosion test products are determined using (EDS), (EPMA) and (XRD).

The results indicate that the hot corrosion resistance of plasma sprayed TBCs is enhanced by laser addition of alumina. This enhancement due to reducing of specific reactive area of composite surface layer and consequently, decreasing the reaction between molten salt and zirconia stabilizers. In addition to elimination of the vertical crack and pores which are in conventional YSZ. SEM indicates that corrosion products have rod-like and semi cubic crystals in both type of coatings. In coating with alumina, these crystals are found fewer and smaller than conventional coating in terms of quantity and size. The semi-cubic crystals grow to needle like structure with increasing of time exposure to form numerous needles in glossy matrix at 40hours. The XRD patterns of conventional and composite coating before and after hot corrosion at different interaction time are clearly formed many extra new phases.  The main phases before corrosion are metastable tetragonal phase (t') and resident of monoclinic phase (m) for conventional YSZ, while for YSZ+Al2O3 composite are (t') and α-Al2O3. Corrosion products are m phase and vanadium compounds (YOV4). The amount of m phase formed is less than the vanadium compounds (YOV4). This observation suggests that during failure there are still high volume fraction of t' phase.  Therefore, the low reaction rate of formation of YOV4 without reaching the m phase underneath plasma sprayed for composite coating and increasing the resistance of corrosion by alumina addition.

Recent Publications

- .Mohammed J. Kadhim, Sami A. Ajeel, Ali M. Resen "Hot corrosion of plasma sprayed and laser sealed coatings of yttria partially stabilized zirconia thermal barrier coatings with molten eutectic vanadate-sulfate Salt": 2nd international conference of material chemistry 13-14 July, Vol. 6, no. 5, pp. 76, berlin, Germany (2017)  .

365: 519-530.

- A. Keyvani, M. Saremi and M. Heydarzadeh, "Microstructural stability of zirconia–alumina composite coatings during hot corrosion test at 1050 oC," Journal of Alloys and Compounds , vol. 506 , p. 103–108, 2010.

- H. Habibi and S. Guo, "Evolution of Hot Corrosion Behavior of YSZ-Ta2O5 Composites with Different YSZ/Ta2O5 Ratios," Journal of Applied Cerammic Technology, vol. 12, no. 3, pp. 542-550, 2015.

Ali Mezher Resen is a PhD student in Production Engineering and Metallurgy, University of Technology, Baghdad, Iraq. He is working as a Lecturer at the same school where he is studying. He obtained his Bachelor’s in Metallurgy Engineering in 2004, and he got his MSc in Metallurgy Engineering in 2008. He had studied Surface Engineering for PhD and the thesis subject was laser processing and thermal barrier coating material, plasma spray  . He has contributed greatly to the understanding of surface engineering of materials and coating material. Also he is a member in many scientific societies and has published many research articles in his field.

Email: alimizhir@yahoo.com

Notes/Comments: