Peculiarities of refractory metal borides formation during mechanical  alloying

Mariia P.Savyak, PhD, IPMS, Ukraine

Abstract

Powdered mixtures of transition IY-YI group metals and boron were milled in a planetary mill at a rotational speed of a disk 735 rev/min and a vial speed — 1840 rev/min. The steel balls to powder mass ratio was 20:1, X-ray analysis was carried out on the installation DRON3 in copper Ka radiation. Refractory compounds borides were shown to form during mechanical alloying through the following mechanisms: a) mechanically induced self-propagating reaction; b) formation of new phase nuclei and their growth and c) formation  of  interstitial boron-in-metal  solid solutions, their subsequent decomposition  and the appearance of the МеВ2 phases.

The mechanism of mechanically induced self-propagating reaction is determined by the enthalpy of refractory compound formation and the ability of substitutional solid solution formation ( if two or three boron atoms  take place instead  metal atoms knocked out of  the crystal lattice  by milling).

The formation of interstitial solid solutions was only observed for bcc metals, which  is related to the far bigger free volume of the bcc  structure as compared to that of the close-packed hexagonal one and depends  on the relationship between the radii of metal and non-metal (Hagg’s rule)

Recent Publications

- M.P. Savyak at al. (2018) Mechanical Synthesis of Tantalum Borides and Modeling of Solid Solutions of Boron in Tantalum, Powder Metallurgy and Metal Ceramics, December 2018.

- M.P. Savyak at al. (2018) Mechanosynthesis of ceramics composite TiC-2TiB2. 10 TH International Conference: Advanced Materials and Technologies.24-26 oct., 2018 Ninghai, China.

- Maria P. Savyak at al. (2016) Crystallographic Features of Nanosized Titanium Carbide Produced from Titanium and Carbon in a Planetary-Ball Mill. Powder Metallurgy and Metal Ceramics 55(5-6) Oct 2016.

- Maria P. Savyak at al. (2015) Mechanosynthesis of Nanodispersed Titanium Diboride .Powder Metallurgy and Metal Ceramics 53(9-10) February 2015.

- M.P. Savyak, I.V. Uvarova, T.M. Yarmola (2008) Using non-equilibrium state in the MoO3-H-C system for low temperature synthesis of ultradispersed molybdenum carbide powders. Processing and Application of Ceramics, 2 [2] (2008) 97–102.

- Maria P. Savyak at al. (2004) Electrochemical hydrogenation of Mg 65Cu 25Y 10 metallic glass Journal of Alloys and Compounds 364(1):229-237.

Biography

Dr. Maria P. Savyak currently works at the I. M. Frantsevich Institute for Problems of Materials Sciences, National Academy of Sciences of Ukraine.

Her present research interests include non-equilibrium processing for synthesis of nanocrystalline refractory compounds. Maria does research in Electrochemistry, Materials Chemistry and Physical Chemistry. Their current project is "Using mechanical alloying to formation of refractory compounds, metallic alloys, MAX- phases: Ti3AlC2, Ti2AlC, Cr2AlC, Ti3SiC2.

https://www.researchgate.net/profile/Maria_Savyak

Email: mari_saviak@ukr.net

Notes/Comments: