Abstract

Effect of silica and lignocellulosic additives on the formation and the distribution of meso and macropores in foam metakaolin-based geopolymer filters for dyes and wastewater filtration

Martine Youmoue*1,2, Rufin Théophile Tene Fongangc3, Ameni Gharzouni2, Rodrigue Cyriaque Kaze4, Elie Kamseu3, Vincenzo M Sglavo5, Ignas Kenfack Tonle1, Benoit Nait-Ali2, Sylvie Rossignolb*

1RU-NOCHEE, Research Unit of Noxious Chemistry and Environmental Engineering, Faculty of Science, University of Dschang, P.O. Box 67 Dschang, Cameroon.

2Institut de Recherche sur les céramiques (IRCER), UMR CNRS 7315, CEC, Université de Limoges, 12 Rue Atlantis, Limoges, France.

3Local Materials Promotion Authority (MIPROMALO), P.O. Box 2396 Yaounde, Cameroon.

4Laboratory of Applied Inorganic Chemistry, Faculty of Science, University of Yaoundé I, P.O. Box 812, Yaoundé, Cameroon.

5Department of Materials Engineering and Industrial Technologies, University of Trento, Via Mesiano 77, 38050 Trento, Italy.

Corresponding authors : youmstina@yahoo.fr or martine.youmoue@univ-dschang.org (M. Youmoue*),  sylvie.rossignol@unilim.fr (S. Rossignol*)

Keywords: meso and macro pores, silica, lignocellulosic, geopolymers, foams, filters.

- Abstract body

This work investigates how silica and lignocellulose additives affect the production of metakaolin based-geopolymer foam filters. Lignocellulosic material from wood powder sawdust (S), silica from rice husk ash (RHA), calcined (Sa) and uncalcined (Sab) sand were separately used together with high amorphous silica fume (FS) (foaming agent) and integrated into the matrix (metakaolin and solution). The different geopolymer pastes were cured at 70 °C to enhance the pore formation. Results presented the geopolymer foams filter as sponge-like composites having 58-68 % of porosity with 1-4 MPa of compressive strength. RHA and Sa lead to materials with more meso and macropores. Sawdust based-geopolymer (the hardest foam) containing channel pores predominated by coarse pores exhibited a flow rate of 4 mL/min. The absence of the bands of MB from FT-IR spectra and UV spectra (663 nm) of MB filtrate (totally blue discoloured) indicated that, geopolymers foams filters designed are suitable for dyes and wastewater filtration.

- Image

- References

- M. Xu, Y. He, C. Wang, X. He, X. He, J. Liu, X. Cui, Applied Clay Science Preparation and characterization of a self-supporting inorganic membrane based on metakaolin-based geopolymers. 2020. Appl. Clay Sci.115. 4–9.

- E. Prud, P. Michaud, E. Joussein, C. Peyratout, A. Smith, S. Arrii-clacens, J.M. Clacens, S. Rossignol. 2010. Silica fume as porogent agent in geo-materials at low temperature, J. Eur. Ceram. Soc. 30. 1641–1648.

- Bai. C. and Colombo. P. 2018. Processing, properties and applications of highly porous geopolymers: a review Ceramics International, 44 (Issue 14), 16103-16118.

- Biography

Martine YOUMOUE is finalysing her p.hD program at the University of Dschang, Cameroon. She is supervised by prof Ignas TONLE KENFACK at the University at the Dschang and Prof Elie KAMSEU at MIPROAMALO (Local Material Promotion Authorithies) Cameroon. After many internships at MIPROMALO, she obtained AUF (Agence Universitaire de la Francophonie) doctorate scholarship, which allowed her to do three visits (five months each) at IRCER (Institut de Recherche sur les Ceramiques), Limoges, France. Those internships were supervised by Prof Sylvie Rossignol. Martine YOUMOUE has three papers in her active (one published in Ceramic International, one accepted in Ceramic and Modern Technology, and the current work accepted for publication in SN Applied Science).

- Presenting author details

Full Name: Martine Youmoue

Contact number: +1 2406107842/+237695736761

Twitter account: @ Martina Youms

LinkedInaccount: https://www.linkedin.com/in/martine-youmoue-4597b87a

Session name: Material Science and Technology

Category: Oral presentation

Passport Number: 0994960