# Assessment of thermal annealing on structural, electrical, optical and surface topographical features of titania films for solar cells

Reema Agarwal1,2,*, Himanshu2, S.L. Patel2, C. Ameta1 and M.S. Dhaka2

1Department of Chemistry, Mohanlal Sukhadia University, Udaipur 313001, India

2Department of Physics, Mohanlal Sukhadia University, Udaipur 313001, India

Abstract

Titanium dioxide or titania (TiO2) has profoundly attracted the academia and industries due to its unique physical and chemical characteristics and diverse applications from solar cells to photocatalyst. The titania films have different roles in CdTe, perovskite, dye sensitized and organic solar cells as window/buffer layer, electron transport layer, photoelectrode etc. In order to further improve the stability and performance of these solar cells, the advancement in properties of titania films is essential which can be done by thermal annealing. The present work reports an assessment on thermal annealing induced structural, electrical, optical and topographical features/properties of e-beam evaporated titania films which are annealed in range of 100-500ºC for one hour. XRD analysis reveals a phase transformation from amorphous to crystalline beyond 300°C. Electrical measurements unveil the ohmic nature and increment in resistivity for annealed films vis-à-vis to pristine. Optical properties indicate high transparency of all films where their optical energy band gap lies in range of 3.53-3.69 eV. Surface topographical study demonstrates changes in average and RMS roughness with the treatment. The assessment shows that titania films annealed at 500ºC have crystalline nature (with improved crystallinity), higher transmittance (in visible region), suitable band gap and ohmic nature, thus, these could be recommended for window and electron transport layer applications in solar cells.

Keywords: Titania films; E-beam evaporation; Buffer layer; Crystallinity; Transmittance.

Corresponding author: r.reemaagarwal@gmail.com