Mechanochemical-assisted Synthesis of Ternary Sulfide Embedded in Carbon for Efficient Hydrogen Evolution reaction

Tian (Leo) Jin, PhD, Department of Applied Chemistry, Xi’an Jiaotong University, Xi’an, PR China

Xiaofei Liu, Key Laboratory for Advanced Materials and Research Institute of Industrial Catalysis, East China University of Science and Technology, Shanghai, PR China

Wangcheng Zhan, PhD, Key Laboratory for Advanced Materials and Research Institute of Industrial Catalysis, East China University of Science and Technology, Shanghai, PR China

Yanglong Guo, PhD, Key Laboratory for Advanced Materials and Research Institute of Industrial Catalysis, East China University of Science and Technology, Shanghai, PR China

Yanfeng Zhang, PhD, Department of Applied Chemistry, Xi’an Jiaotong University, Xi’an, PR China

Abstract

Hydrogen energy, with high energy density and clean emission, has attracted significant attention in scientific community due to their potential as a way to reduce reliance on traditional fossil fuels. Hydrogen evolution reaction (HER), a cathodic process in water electrolysis, provides a green and efficient way for sustainable hydrogen generation. In this work, we adopt a facile synergistic coupling strategy to synthesize ternary sulfide RuNiS nanohybrids with an intriguing morphology featuring highly-dispersed RuNiS nanocrystalline embedded in carbon matrix. The key to our success lies in the utilization of mechanochemical-assisted synthesis, which can not only obtain highly-dispersed metal sulfide nanocrystalline, but also facilely tailors the electronic structure with variable active sites. Owing to the well-controlled structure, abundant active sites and synergistic effects between multiple metal sites, the composite exhibits excellent performance for HER in both alkaline and acid electrolytes. To our delight, RuNiS-N/C delivers a small overpotential of 25 mV at the current density of 10 mA cm−2 in 1 M KOH, outperforming the benchmark Pt/C catalyst. Meanwhile, such RuNiS-N/C also shows excellent activity in 0.5 M H2SO4, with a small overpotential of 43 mV at the current density of 10 mA cm−2. Therefore, the mechanochemical-assisted synergistic coupling strategy provides new opportunities for the development of highly efficient HER electrocatalysts.

Figure 1. The synthesis of ternary RuNiS-N/C via a facile mechanochemical-assisted synergistic coupling strategy.

Figure 2. (a) HER polarization curves of the RuS-N/C, NiS-N/C, RuNiS-N/C and Pt/C, respectively. (b) Tafel plots of corresponding RuNiS-N/C and Pt/C. (c) Polarization curves of the RuNiS-N/C catalyst decorated on GC electrode before and after 1000 CV cycles. (d) Long-term HER stability test of the RuNiS-N/C at current-time chronoamperometric. All tests are performed in 1 M KOH.

Recent Publications (minimum 5)

- Hu C, Dai L (2017) Multifunctional Carbon-Based Metal-Free Electrocatalysts for Simultaneous Oxygen Reduction, Oxygen Evolution, and Hydrogen Evolution. Advanced Materials 29:1604942

- Xu JY, Liu TF, Li JJ, Li B, Liu YF, Zhang BS, Xiong DH, Amorim I, Li W, Liu LF (2018) Boosting the hydrogen evolution performance of ruthenium clusters through synergistic coupling with cobalt phosphide. Energy & Environmental Science 11: 1819-1827.

- Liu XF, Hood ZD, Zheng Q, Jin T, Foo GS, Wu ZL, Tian CC, Guo YL, Dai S, Zhan WC, Zhu HY, Chi MF (2019) Optimizing the structural configuration of FePt-FeOx nanoparticles at the atomic scale by tuning the post-synthetic conditions. Nano Energy 55: 441-446.

- Jin T, Sang XH, Unocic RR, Kinch RT, Liu XF, Hu J, Liu HL, Dai S (2018) Mechanochemical‐Assisted Synthesis of High‐Entropy Metal Nitride via a Soft Urea Strategy. Advanced Materials 30: 1707512.

- He WH, Ifraemov R, Raslin A, Hod I (2018) Room-Temperature Electrochemical Conversion of Metal–Organic Frameworks into Porous Amorphous Metal Sulfides with Tailored Composition and Hydrogen Evolution Activity. Advanced Functional Materials 28: 1707244.

Biography

Tian (Leo) Jin is a lecturer in Chemistry at Xi’an Jiaotong University. He received his PhD in physical chemistry from East China University of Science and Technology in 2018. His research involves rational design and synthesis of novel porous materials such as porous organic polymers and metal-organic frameworks for energy-related applications like separations and electrochemical catalysis.

Email: tianjin.ecust@gmail.com