# Nano-meso-macro: Hierarchical Superstructures synthesized in Bicontinuous microemulsions for electrocatalysis and SERS

Margarita Sanchez-Dominguez, PhD, CIMAV Monterrey, MEXICO

### Abstract

Statement of the Problem: Hierarchical superstructures (HSSs) are 3-D structures with a significant improvement in some properties as compared to isolated nanoparticles. However, formation of HSSs has been conducted by intricate methods that usually involve synthesis of the building blocks and the assembly in superstructures in a second step. Methodology & Theoretical Orientation: As alternative one-pot procedure, we propose the use of bicontinuous microemulsions (BCME). The channels of BCMEs have a thickness in the nanometer scale. Both water and oil channels are continuous phases, having infinite lengths. Thus, it is feasible to imagine the growth of HSS inside them, as the narrow thickness of the channels will allow the formation of nanometer building blocks, whilst their interconnection allows for the self-assembly of these nanoparticles into macroscopic 3D networks. The use of BCME for the synthesis of inorganic nanomaterials is rare, in comparison to the use of W/O and O/W ME. When BCME were used, isolated and well dispersed NPs has been obtained, mostly using ionic surfactants and water-soluble precursors. In this investigation, we used BCME based on the nonionic system water/ Synperonic 91/5 /isooctane for the synthesis of Pt, PtCo3O4, PtCoNi,  and Ag HSSs. The use of both water- and oil-soluble precursors were compared. Findings: HSSs resembling nanocorals, made by interconnected NPs or nanoneedles were obtained (Pt, PtCo, PtNi, PtCo3O4), both by chemical reduction and electrodeposition. These materials were explored as electrocatalysts. On the other hand, for Ag superstructures, it was necessary to add a stabilizer (sodium citrate) in order to form a Ag HSS, which was assessed as Surface Enhanced Raman Spectroscopy (SERS) substrate, resulting in analytical enhancement factors in the order of 109 for Rhodamine 6G.  These results demonstrate the usefulness of employing certain BCME for HSSs synthesis of, although the concept is not universal to all BCMEs.

### Image

Figure 1. Synthesis of nano-coral Pt hierarchical superstructures in bicontinuous microemulsion for electrocatalysis.

Recent Publications (minimum 5)

- Adesuji ET, Khalil L, Videa M, Sanchez-Dominguez M (2020). From nano to macro: Hierarchical Platinum Superstructures synthesized using bicontinuous microemulsion for hydrogen evolution reaction. Electrochimica Acta 354: 136608.

- Adesuji ET, Torres-Guerrero VO, Arizpe Zapata A, Videa M, Sanchez-Dominguez M, Fuentes KM (2020). Bicontinuous microemulsion as confined reaction media for the synthesis of plasmonic silver self-assembled hierarchical superstrutures. Nanotechnology 31: 425601.

- Adesuji ET, Guardado-Villegas E, Fuentes KM, Sanchez-Dominguez M, Videa M. Pt-Co3O4 Superstructures by One-Pot Reduction/Precipitation in Bicontinuous Microemulsion for Electrocatalytic Oxygen Evolution Reaction. Catalysts 10: 1311

- Rivera-Rangel RD, Navarro-Segura ME, Arizmendi-Morquecho AM, Sanchez-Dominguez M (2020). Electrodeposition of plasmonic bimetallic Ag-Cu nanodendrites and their application as surface-enhanced Raman spectroscopy (SERS) substrates. Nanotechnology 31: 465605.

- Torres-Guerrero VO, Adesuji ET, Arizpe-Zapata JA, Fuentes K, Pineda-Aguilar N, Videa M, Sanchez-Dominguez M (2020). Synthesis of silver hierarchical superstructures in bicontinuous microemulsion and their application as SERS substrates, IEEE Xplore: 2019 IEEE International Conference on Applied Science and Advanced Technology (iCASAT 2019).

Biography

Margarita Sánchez-Domínguez received a Ph.D. in Physical Chemistry from University of Bristol in 2004. She was a postdoctoral researcher at Institute Charles Sadron (CNRS, Strasbourg, 2004-2006), and at the Institute of Advanced Chemistry of Catalonia (IQAC-CSIC, Barcelona, 2006-2010). She joined CIMAV Monterrey (México) in 2010. She has published around 70 papers, several book chapters, one book and several patents. Her research goal is to understand the interfacial and colloidal properties of surfactant systems with the aim of using them for applications related with materials science and industrial formulations, with a particular focus on the use of bicontinuous microemulsions as confined reaction media for the synthesis of plasmonic hierarchical superstructures for their use as SERS substrates and electrocatalysts. Other interests include drug delivery and stimuli-responsive surfactant systems.

Email: margarita.sanchez@cimav.edu.mx

Notes/Comments: Colaborators:   Videa M,   Adesuji ET, Fuentes KM,   Torres-Guerrero VO, Arizpe Zapata A,  Arizmendi-Morquecho AM,  Khalil L, Basilio K, Guardado-Villegas E.  Funding : CONACYT, FC-2016/1700