LARGE-AREA NANOPARTICLE DEPOSITION USING GAS AGGREGATION PROCESS

H. Nizard1,2, T. Modes2, S. Rauer3, D. Gloess2, P. Frach2, G. Gerlach1

1 Solid State Electronics Laboratory (IFE), TU Dresden, Helmholtzstr. 10, 01069 Dresden, Germany
2 Fraunhofer FEP, Winterbergstr. 28, 01277 Dresden, Germany
3 University of Applied Sciences, Dr.-Friedrichs-Ring 2A, 08056 Zwickau, Germany

ABSTRACT

The continuous growth of academic interest for nano-fabrication topic since the mid-90‘s is also observed in the steady growth of granted patents and gives hope for a future potential industrial applicability.

The gas aggregation process is a pertinent process, overcoming the limitations of both wet-chemical methods and of mask lithography (speed, deposition area). This process can be combine with standard vacuum deposition processes and integrated into standard vacuum deposition tools, but must be up-scaled to large-area deposition for industrial applications.

Gas aggregation setup established in collaboration between TU Dresden (IFE) and FEP consists in a gas-flow-sputtering nanoparticles source (Hollow cathode), a PECVD matrix deposition source, an Etching unit, and a 4th station for possible extension (Magnetron Sputtering Matrix deposition or CNT deposition by ESI)

The originality of this setup lies in its dimensions (aggregation volume ≈ 100L; up to 3slm gas flow) Adjustable slit opening between aggregation and deposition zones, allowing a 12mm wide Plane jet in the dynamic vacuum setup, translating in up to 20mm wide nanoparticle deposition.

After presenting the technical setup and its operation principle, this work will show obtained results for the deposition of Ag NP – SiOx Metal-polymer nanocomposites (Deposition rate 15…60nm/min)