ABSTRACT

PbS:CuO, alloyed thin films were successfully deposited on glass substrates  under the deposition condition of 40oC of  NaOH solution, using two solution based methods: successive  ionic layer  adsorption and reaction (SILAR) and solution growth technique. The crystallographic studies were done using X-ray diffractometer (XRD) and scanning electron microscope (SEM).  The deposited alloyed samples were annealed  at 250oC  and 1500C.  using Master Chef Annealing Machine. Rutherford backscattering Spectroscopy (RBS) analysis confirmed the  percentage of the elements of copper, lead, sulphur and oxygen in  the alloyed thin films. The optical characterization was carried out using UV-1800 double beam spectrophotometer.  Sample pc1  annealed at 250 oC has an optical transmittance of 27% -70% in the ultraviolet region, 71%-85% in the visible and 84%-88% in the near infrared regions of electromagnetic spectrum.  The alloyed thin films of samples pc2 of PbS:CuO annealed at 150oC, shows optical transmittance of 15%-60% in the ultraviolet region, 61%-59% in the visible, and 60%-58% in the near-infrared regions of electromagnetic spectrum. The two samples, have  equal direct wide  band gap of 3.45±0.05eV. From the spectral qualities, these compound alloyed  thin films   may be found useful in cold and heat mirror applications, active layer in various types of solar cells and  passive layer in heat and cold mirror application, vulcanization in tyre production due its thermal stability, active layer in various types of solar cells, liquid crystal displays, flat panel displays  for opto-electronic applications and gas censor applications.