# As3+ detection using nanostructured MnOx and phase evolution of the active material during sensing

Tanvi Gupte, Indian Institute of Technology, India

### Abstract (300 word limit)

Statement of the Problem: Arsenic (As) contamination is a serious concern, affecting over 140 million people worldwide. Use of As-contaminated water for the preparation of food, irrigation of crops, and drinking has serious consequences on health. Therefore, accurate and selective detection of As in water is important. A simple, one-step electrodeposition approach was used to fabricate MnOx on indium doped tin oxide (ITO) substrate for highly sensitive As detection.  The stripping-voltammetry-induced changes in nanostructures and oxidation states are studied by performing several characterization studies before and after sensing.

Methodology: The phase and morphology of MnOx were controlled by the cyclic voltammetry (CV) technique. The electrodes were characterized by electron microscopy, spectroscopy, and electrochemical techniques. Selectivity of the electrode for As3+ was studied in the presence of 10 times higher concentrations of several metal ions.

Findings: We report an experimental limit of detection of 1 ppb through anodic stripping voltammetry (ASV). The electrode is selective to As3+. Additionally, we report the simultaneous phase evolution of active material occurring through multiple stripping cycles, wherein MnO/Mn2O3 eventually converts to Mn3O4; as a result of change in the oxidation states of manganese. This occurs with concomitant changes in morphology. Change in the electronic property (increased charge transfer resistance) of the material after multiple stripping cycles, eventually decreases sensitivity.

Conclusion & Significance: This work successfully established electrochemical detection of trace amount of arsenite (~ 1 ppb) which is below the WHO guideline value for As(III) in drinking water (10 ppb). The electrode is capable of interference-free As3+ detection in alkaline medium. A detailed insight is provided about the fundamental, yet unexplored, issue of phase evolution and morphological changes in the nanosystem during electrochemical sensing. This is a crucial contributing factor for limiting the performance of electrochemical sensors in the course of their operation.

### Image

Figure: Phase and morphological evolution of nanostructured manganese oxide-based electrodes during multiple arsenic sensing cycles.

Recent Publications (minimum 5)

- Highly-sensitive As3+detection using electrodeposited nanostructured MnOxand phase evolution of the active material during sensing, Tanvi Gupte, Sourav Kanti Jana, Jyoti Sarita Mohanty, Pillalamarri Srikrishnarka, Sritama Mukherjee, Tripti Ahuja, Chennu Sudhakar, Tiju Thomas, and Thalappil Pradeep, ACS Appl. Mater. Interfaces, 11 (2019) 28154−28163

- Arsenic in and Water: Speciation, Sources, Distribution, and Toxicology, Tanvi Gupte, Sritama Mukherjee, Shantha Kumar Jenifer, Tiju Thomas, and Thalappil Pradeep, Encyclopedia of Water: Science, Technology and Society, John Wiley & Sons, (2019) DOI: 10.1002/9781119300762 (eBook ISBN: 9781119300762)

- Arsenic in Water: Fundamentals of Measurement and Remediation, Sritama Mukherjee, Tanvi Gupte, Shantha Kumar Jenifer, Tiju Thomas, and Thalappil Pradeep, Encyclopedia of Water: Science, Technology and Society, John Wiley & Sons, (2019) DOI: 10.1002/9781119300762 (eBook ISBN: 9781119300762)

- Design and evaluation of artificial cornea with core–skirt design using polyhydroxyethyl methacrylate and graphite, Mukty Sinha and Tanvi Gupte, International ophthalmology, 38 (2018) 1225-1233.

Biography (150 word limit)

Tanvi Gupte has an academic background in pharmacy, followed by post-graduation in Medical devices. As a part of her PhD, she is currently focused on developing  electrochemical, cellular and non-cellular sensors for the detection of arsenic. This will also help in creating awareness and importance of clean water. She strives to make a social impact with her research.

Email: tanvi.gupte@yahoo.com

Notes/Comments: