Zr alloy protection against high-temperature oxidation: double-layered coating with active and passive functional properties

Irena Kratochvílová*1, Petr Ashcheulov1, Radek Škoda2, Jaromír Kopeček1, Jan Macák3, Adéla Nováková4, Johannes Neethling5, Peng Xu6, Jan Lorinčík7 and Martin Steinbrück8.

1Institute of Physics of the Czech Academy of Sciences, Na Slovance 2, CZ-182 21, Prague 8, Czech Republic

2Czech Technical University in Prague, Czech Institute of Informatics, Robotics and Cybernetics, Jugoslávských partyzánů 1580/3, Prague 6, CZ-160 00, Czech Republic

3University of Chemistry and Technology, Power Engineering Department, Technická 3, Prague 6, CZ-166 28, Czech Republic

4Faculty of Nuclear Physics and Physical Engineering, Czech Technical University in Prague, Zikova 1, 160 00 Prague 6, Czech Republic

5Centre for HRTEM, Department of Physics, Nelson Mandela University, Port Elizabeth, South Africa

6Nuclear Fuel Division, Westinghouse Electric Company, 5801 Bluff Road, Hopkins, SC 29209, USA

7Research Centre Řež, Hlavní 130, CZ-250 68 Husinec-Řež, Czech Republic

8Institute for Applied Materials (IAM), Karlsruhe Institute of Technology, Hermann-von-Helmholtz-Platz 1, 76344 Eggenstein-Leopoldshafen, Germany

### Keywords: polycrystalline diamond,  Zr alloy protection against corrosion, CrAlSin coating

- Abstract:

In this work we investigated the hot steam oxidation of ZIRLO fuel cladding coated with a double layer consisting of 500 nm nanocrystalline diamond (NCD) as the bottom layer and 2 m chromium-aluminum-silicon nitride (CrAlSiN) as the upper layer. Coated and noncoated ZIRLO samples were exposed for 4 days at 400 °C in an autoclave (working water-cooled nuclear reactor temperature) and for 60 minutes at 1000 °C (nuclear reactor accident temperature) in a hot steam furnace. We have shown that the NCD coating protects the Zr alloy surface against oxidation in an active way: carbon from NCD layer enters the Zr alloy surface and, by changing the physical and chemical properties of the Zr cladding tube surface, limits the Zr oxidation process. In contrast, the passive CrAlSiN coating prevents the Zr cladding tube surface from coming into physical contact with the hot steam. The advantages of the double layer were demonstrated, particularly in terms of hot (accident-temperature) oxidation kinetics: in the initial stage, CrAlSiN acts as an impermeable barrier, but after a longer time, the protection by CrAlSiN decreases as an increasing number of cracks in the carbon of NCD penetrate the Zr cladding surface and worsen conditions for Zr oxidation. For the double-layer coating, the underlying NCD layer mitigates thermal expansion, reducing cracks and defects in upper layer CrAlSiN.

- Image:

- Reference:

1. Skarohlid, J. et al. Nanocrystalline diamond protects Zr cladding surface against oxygen and hydrogen uptake: Nuclear fuel durability enhancement. Scientific Reports 7, 14, doi:10.1038/s41598-017-06923-4 (2017).

2. Ashcheulov, P. et al. Thin polycrystalline diamond films protecting zirconium alloys surfaces: From technology to layer analysis and application in nuclear facilities. Applied Surface Science 359, 621-628, doi:10.1016/j.apsusc.2015.10.117 (2015).

### Biography:

As.prof. Irena Kratochvilova  obtained very important results which were published in prestigious journals and were cited by scientific community. She has published 85 papers in impacted journals.  She has been working in the Institute of Physics AS CR and teaching at the Faculty of Nuclear Engineering Czech Technical University.

### Presenting author details

Full Name: Irena Kratochvilova

Session name/ number:

Category: Oral presentation