Abstract Category:Physical Medicine & Rehabilitation, Orthopedics, Trauma

Title:Comparison of Mechanical Properties of Nonridged Versus Ridged Backslabs in Lower Limb Fractures

Muhammad Maaz Gul Kaka Khel(Trauma and Orthopaedics, Liverpool University Hospitals Foundation Trust, Liverpool, GBR),Syed Naveed Mohsin(Trauma and Orthopaedics, Saint James's Hospital, Dublin, IRL),Faisal Shahzad(Orthopaedic Unit-1, Mayo Hospital, Lahore, Lahore, PAK),Philip Purcell(Centre of Applied Science for Health, Technological University Dublin, Dublin, IRL),Amir Siddique(Trauma and Orthopaedics, Our Lady of Lourdes Hospital, Drogheda, IRL),Mahmood Ahmad(Trauma & Orthopaedics, Shifa International Hospital Islamabad, Islamabad, PAK),Muhammad Shahab(Trauma and Orthopedics, Royal Bolton Hospital, Bolton, GBR)

Corresponding/Presenting author details: Muhammad Maaz Gul Kaka Khel,maaz.cpsp@gmail.com,07931563140,5 cavalier drive Blacon Chester UK.

Introduction : Lower limb fractures frequently require immobilization with backslabs to promote healing. This study investigates a novel approach involving the incorporation of a single ridge to enhance backslab strength while maintaining cost-effectiveness.

Objective: To assess the mechanical performance of ridged backslabs in comparison to traditional nonridged backslabs, specifically focusing on their load-bearing capacity and cost-effectiveness when used in lower limb fractures.

Methods: This experimental study, conducted between January 2023 and June 2023, compares three groups backslabs with varying layers(eight,ten and twelve) were fabricated, each consisting of four ridged and four non-ridged specimens. These backslabs, constructed from six-inch plaster of Paris rolls, were 190 cm in length. A three-point bending test was conducted on both groups using a Hounsfield H100KS Universal Testing Machine, with a crosshead speed of 5 mm/min and a span distance of 190 mm between supports.

Results: Significant differences in mean maximum force endured were observed between the ten-layered and twelve-layered flat and ridged backslabs (p-values: 0.003 and 0.004, respectively). Ten-layered ridged backslabs exhibited a 56 N higher load-bearing capacity, while twelve-layered ridged backslabs withstood 73.9 N more force than their flat counterparts, underscoring the superior strength of ridged lower limb backslabs.

Conclusion: Ridged backslabs outperformed non-ridged backslabs in terms of strength when subjected to external forces. These findings support the potential adoption of ridged backslabs as a lightweight, costeffective, and robust alternative for immobilization in lower limb fractures.

Keywords: non ridged backslab, lower limb cast, plaster cast, load to failure, ridged backslab