Title: Synthesis and characterization of porous functionalized MCM-41 nanoparticles for application in drug delivery

Negar Pourzadi*, Zahra Shariatinia

Department of Chemistry (Inorganic Chemistry) Amirkabir University of Technology

(Tehran Polytechnic)

Keywords: MCM-41, mesoporous nanoparticles, Cyclophosphamide, Controlled drug release

- Abstract Body

Cyclophosphamide is one of the most effective drugs used to treat various types of cancer, However, its applications are limited due to the high toxicity and rapid metabolism. On the other hand, nanotechnology has many potential applications in the field of cancer treatment, for example, in order to increase the therapeutic effects of anticancer drugs, nanosystems with high bioavailability, biodegradability and biocompatibility have been developed. Among these nanosystems, functionalized mesoporous nanoparticles (MSNs), due to their benefits, are progressing rapidly in the field of targeted cancer treatment. In this study, MCM-41 meso-silica nanoparticles were synthesized with 10% to 50% of tert-Butylamine. Then Cyclophosphamide was loaded into functionalized MCM-41. The surface area, pore size and pore volume of MCM-41 were measured equal to 917 m2/g, 106Å and 2.08 cm3/g but those of functionalized MCM-41 were considerably smaller, shows that Amino groups are in the cavities of these nanoparticles.

The release of Cyclophosphamide was significantly increased in about 24h (burst release) but after that the drug release showed a slow enhance within 7 days (sustained release). Finally, it was concluded that functionalized MCM-41 with 30% tert-Butylamine was the most promising drug delivery system as it had improved biocompatibility, mechanical and drug release properties. Drug release was investigated in acidic, alkaline and neutral environments. Most of its release occurred in a neutral environment, moderate in alkaline medium and the lowest in acidic media.  At last, the kinetic models of drug release, including the zero-order, first-order, Higuchi, and Korsmeyer-pepas reactions, were studied and the release of Cyclophosphamide from the functionalized nanoparticles MCM-41was most similar to the Koresymer-Pepas model.

- Image:

- Reference:

1.               Delpeuch, A. Leveque, D. Rob, L. et al. “Off-label use of oxaliplatin in

patients with metastatic breast cancer”. Anticancer Res; 31(2011): 1765-7.

2.               Wang C, Bao X, Ding X, et al “A multifunctional self-dissociative

polyethyleneimine derivative coating polymer for enhancing the gene

transfection efficiency of DNA/polyethyleneimine polyplexes in vitro and in

vivo”. Polym Chem. 6(2015):780–796.

3.              Nanoparticles, A.M. Lara, G.G. Fernandes, M. et al “Response of Fibroblasts

MRC-5 to Flufenamic Acid-Grafted MCM-41 Nanoparticles. Bioengineering                  5, 4(2018).

IV.     Biography                                                                Negar Pourzadi has completed her BSc from ShahidBeheshti University in Iran at the age of 24 years from then she started her MSc in Inorganic Chemistry in Amirkabir University of Technology in Iran.

V.          Presenting author details

Full name: Negar Pourzadi
Contact number: 989128305224
Twitter account:
Linked In account:

Session name/ number: drug delivery Techniques
Category: Oral presentation