Study on the Effect of Enzyme Treated Fibers α-cellulose on the Mechanical Properties of Starch Blends

Chi-Yuan Huang a，Che-Wei Lin，Mei-Chuan Kuo

Department of Materials Engineering, Tatung University, Taipei, Taiwan

a.cyhuang@ttu.edu.tw

I.   Abstract.

In this study, the biodegradable materials were prepared by using sebacic acid modified Tapioca starch as the substrate, and then biodegradable plastics (Ecoflex) and α-cellulose were added to study the effect of adding α-cellulose on the properties of the material. This study investigated the mechanical properties of α-cellulose on biodegradable materials after treatment with 4 Vol% fiber enzyme (Cellic CTec3) at different temperatures (35, 45 ° C) for different hours (24, 30, 36, 42 hr). The material morphology was examined by scanning electron microscopy (SEM). After adding MCC or NCC hydrolyzed α-cellulose to biodegradable materials, MCC and NCC promote starch to crystallize, so the elastic modulus and stress value of the material are greatly increased. After α-cellulose was treated by enzymes with higher temperature and longer treatment time, there were much more MCC or NCC to produce, they will make the starch crystallize eases . The optimum condition in this experiment is α-cellulose was treated with 4Vol% of Cellic CTec3. The good material properties in this study was adding MCC or NCC formed (45° C,36hrs) to the starch/biodegradable blend.

II.   Image

III.	Biography

Che-Wei Lin will graduate from materials engineering of Tatung University as master degree.I am major in biodegradable materials. I am currently a teaching assistant of materials experiment

IV.	Presenting author details

Full Name: Che-Wei Lin

Contact number: +886932203966

Session name/ number: Polymer Material Science and Engineering

Category:  Poster presentation

Passport Number: 314098218