Recycling of galvanic copper sludge for pure copper production

### NATTHICHA M.1,  KHUMKOA K.1,  PANYA B.1,  PIYAWIT W.1,  TAPANY P.1,  THONGNAK S.1, YINGNAKORN T.1

1School of Metallurgical Engineering, Institute of Engineering, Suranaree University of Technology, Nakhon Ratchasima, Thailand

### Keywords: Hydrometallurgy, Electrometallurgy, Electrowinning, Galvanic sludge, Copper cathode

Abstract

Metal containing waste sludge from electronic industrial has been rapidly accumulating due to the surge of global demands for electronic components. This study looks into the feasibility of recycling copper from galvanic waste through hydrometallurgy combining with electrometallurgy process. The parameters of copper selective leaching including types of leaching solution, acid concentrations, and liquid-solid ratios were systematically studied. The optimum selective leaching conditions were 1M and 2M sulfuric acid with 24 hours leaching duration, 100/1000 g/cc solid-liquid ratio offering copper leach recovery of 42,540 and 45,850 mg/l, respectively. Copper purification was successfully obtained from electrolytic refining process. The effects of electrolysis voltage to the amount and purity of copper cathode were studied. It was found that the optimum parameters for copper purification were using 2M sulfuric acid with electrolytic voltage of 2.2V. Under these conditions, the recovery of pure copper was raised up to 92%.

### Biography:

Miss Nathicha Ma-ud has completed his Bachelor degree in Metallurgical Engineering from the School of Metallurgical Engineering, Suranaree University of Technology, Thailand. Present, he is Master student at the same school.

### Presenting author details

Full Name: Miss Natthicha Ma-ud

Contact number:

Twitter account:

Linked In account:

Session name/number: Track 10 Metal Recycling

Category: Oral presentation

Passport Number: