Recycling of Spent Electro-Nickel-Plating Solution by Electrowinning

### PIAMSAK L.1,  KHUMKOA K.1,  PANYA B.1,  PIYAWIT W.1,  TAPANY P.1,  ANUTAI K.1,  LOESLAKKHANA S.1

1School of Metallurgical Engineering, Institute of Engineering, Suranaree University of Technology, Nakhon Ratchasima, Thailand

### Keywords: Hydrometallurgy, Electrowining, Electro nickel plating solution, Industrial waste

Abstract

This research aims to study the feasibility of nickel recovery from spent electroplating solution via hydrometallurgy and electrochemical treatment. The spent nickel plating solution obtained as an industrial waste was found to contain nickel of 89,000 mg/L, which was still in high quantity sufficient for prospective recovery. In this research, precipitation of nickel from the plating solution was first carried to separate other unwanted impurities. The remained nickel precipitates was then leached by using 1 M or 2 M sulfuric acid for 24 hours at solid/liquid ratio of 100 g/L. The leached solution was then adjusted to obtain pH 2 prior to elecgtrowinning. It was found that increasing the acid concentration from 1 M to 2 M resulted in greater amount of nickel in the solution from 11,410 mg/L to 15,630 mg/L. The greater amount of nickel in the leach solution used as the electrolyte in electrowinning is therefore expected to gain greater potential for nickel recovery.

### Biography:

Mr.Piamsak Laokhen has completed his Bachelor degree in Metallurgical Engineering with second class honor from the School of Metallurgical Engineering, Suranaree University of Technology, Thailand. Present, he is Master student at the same school.

### Presenting author details

Full Name: Mr.Piamsak Laokhen

Contact number:

Twitter account:

Linked In account:

Session name/number: Track 10 Metal Recycling

Category: Oral presentation

Passport Number: