# The influence of the degree of crosslinking and column dimension on the lithium isotope separation factor

Jiri Mikes, Ludek Jelinek, University of Chemistry and Technology, Prague, Czech Republic

### Abstract (300 word limit)

There are two naturally occurring lithium isotopes, 6Li at 7.59% and 7Li at 92.41% relative abundance1. The small cross section (0.045 barns)2 of lithium isotope 6Li determines useable its compounds in power industry3. Due large cross section (940barns)2, lithium compound rich in 6Li will be required for the tritium breeder blanket in deuterium-tritium nuclear fusion4. Various methods for lithium isotope separation were invented, and their applicability has been evaluated, for example solvent extraction using macrocycles, laser excitation, thermal diffusion and electro-migration5. One of the suitable methods for lithium isotope separation is ion exchange displacement chromatography6. The separation process can be described as elution chromatography. Large number of influences affects value of lithium isotopes separation factor, column dimension, used mobile phase, temperature etc. Considerable influence can have crosslinking of stabile phase7. All experiments were carried in glass package column (2 m length, i. d. 5 mm). Ammonium chloride 0.5M was used as a mobile phase. Different flow rate of mobile phase in interval 0.1 to 3 mL.min-1 was investigated. As a stabile phase was used poly(styrene-co-divinylbenzene), commercially available as Dowex 50 WX n, where n is crosslinking percentage (2-16%). The narrow particle size fraction (150-200 μm) was prepared commercial resin mean particle size 100-200 mesh by sieving in wet phase. Effects of homogenous particle size, temperature, column dimension and degree of crosslinking on the isotope separation were evaluated.

### Image

Figure 1 factors influencing lithium isotope separation factor α using ion exchange displacement chromatography
Recent Publications (minimum 5)

1.	Coplen, T. B.; Bohlke, J. K.; De Bievre, P.; Ding, T.; Holden, N. E.; Hopple, J. A.; Krouse, H. R.; Lamberty, A.; Peiser, H. S.; Revesz, K.; Rieder, S. E.; Rosman, K. J. R.; Roth, E.; Taylor, P. D. P.; Vocke, R. D.; Xiao, Y. K., Isotope-abundance variations of selected elements - (IUPAC Technical Report). Pure and Applied Chemistry 2002, 74 (10), 1987-2017.

2.	SEARS, V. F., Neutron scattering lengths and cross sectioirn Neutron news 1992, 3 (3), 8.

3.	(a) Hong, S. G.; Greenspan, E., Molten salt cooled encapsulated nuclear heat source (ENHS)-like reactors. Progress in Nuclear Energy 2005, 47 (1-4), 239-250; (b) Nishizawa, K.; Ishino, S.-i.; Watanabe, H.; Shinagawa, M., Lithium Isotope Separation by Liquid-Liquid Extraction Using Benzo-15-Crown-5. Journal of Nuclear Science and Technology 1984, 21 (9), 694-701.

4.	Casini, G., PROGRESS IN STUDIES OF LI17PB83 AS LIQUID BREEDER FOR FUSION-REACTOR BLANKETS. Nuclear Technology-Fusion 1983, 4 (2), 1228-1232.

5.	Symons, E. A., LITHIUM ISOTOPE-SEPARATION - A REVIEW OF POSSIBLE TECHNIQUES. Separation Science and Technology 1985, 20 (9-10), 633-651.

6.	Hagiwara, Z.; Takakura, Y., ENRICHMENT OF STABLE ISOTOPES .3. ENRICHMENT OF 6LI AND 7LI BY ION EXCHANGE COLUMN. Journal of Nuclear Science and Technology-Tokyo 1969, 6 (6), 326-&.

7.	Lee, D. A.; Begun, G. M., THE ENRICHMENT OF LITHIUM ISOTOPES BY ION-EXCHANGE CHROMATOGRAPHY .1. THE INFLUENCE OF THE DEGREE OF CROSSLINKING ON THE SEPARATION FACTOR. Journal of the American Chemical Society 1959, 81 (10), 2332-2335.

Biography (150 word limit)

Jiri Mikes is a Ph.D. student at Department of Power Engineering of University of Chemistry and Technology in Prague. He is a member of research group Water treatment by ion exchange and membrane technologies. His research focuses primarily to lithium isotope separation using ion exchange displacement column chromatography. Except that, he develops automated apparatus for enrichment processes and their prearranging. Jiri Mikes recently published his first article about lithium isotope separation in Journal of radioanalytical and nuclear chemistry. He presented results at international conferences focused on water treatment and ion exchange technologies.

Email: mikesi@vscht.cz

Notes/Comments: