Abstract

MoS2 Nanosheets Covalently Functionalized with Pyrolytically Modified Polyacrylonitrile for Information Storage

- Fei Fan, Bin Zhang, Yaming Cao, Yu Chen*

Key Laboratory for Advanced Materials, Institute of Applied Chemistry, School of Chemistry and Molecular Engineering, East China University of Science and Technology, Shanghai 200237, China. Email: chentangyu@yahoo.com

The electrical conductivity of the laterally ordered polyacrylonitrile (PAN) can be improved by pyrolytic modification. Newly synthesized MoS2 nanosheets covalently grafted with PAN (MoS2-PAN) does not exhibit any electrical switching and memory effect in an ITO/MoS2-PAN/Au device under applied bias voltages. After annealing at 220°C for 4h, the resultant pyrolytically modified product “pyro-MoS2-PAN” shows good nonvolatile rewritable memory performance, with a large ON/OFF current ratio of 4  104 and lower switching on and off voltages of -1.09 and 1.24V. Highly reproducible memory I-V loops of more than 60 consecutive cycles have been achieved without clear degradation of the ON and OFF states. The first oxidation potential of pyro-MoS2-PAN is cathodically shifted over 530mV lower than that of MoS2-PAN, indicating the higher hole injection of pyro-MoS2-PAN when compared to MoS2-PAN. As expected, the non-annealed MoS2/PAN blends–based device does not show any memory effect under the same experimental condition. After annealing at 220°C for 4h, the blends exhibited unstable electrical switching and rewritable memory performance. These results have demonstrated that the electronic properties of polymer functionalized MoS2 nanosheets can be fine-tuned via design-cum-synthesis strategy and thermal annealing approach.

Pyro-MoS2-PAN

Figure 1. (Left) Structure of Pyro-MoS2-PAN and (Right) Consecutive I-V cycles of an ITO/pyro-MoS2-PAN/Au device

References

Y. Chen, B. Zhang, G. Liu, X. Zhuang, E.-T. Kang, Graphene and its derivatives: Switching ON and OFF，Chem. Soc. Rev. 2012, 41(13): 4688–4707

Y. Cao, X. Tian, J. Gu, B. Liu, B. Zhang, S. Song, F. Fan, Y. Chen, Covalent functionalization of black phosphorus with conjugated polymer for information storage, Angew. Chem. Int. Ed. 2018, 57:4543-4548

G. Liu, Y. Chen, S. Gao, B. Zhang, R.-W. Li, X. Zhuang, Recent advances in resistive switching materials and devices: From memories to memristors, Engineered Sci. 2018, 4:4-43