Effect of Mn2+ substitution on optical, structural and magnetic properties of copper ferrites nanoparticles

Talaat M. Hammad a*, S. Kuhnb, Ayman Abu Amsha c, Nasser K. Hejazyd , R. Hempelmannb

a Physics Department, Faculty of Science, Al-Azhar University, P.O. Box 1277, Gaza, Palestine

b Department of Physical Chemistry, Saarland University, 66123 Saarbru¨cken, Germany

c Chemistry Department, Faculty of Science, Al-Azhar University, P.O. Box 1277, Gaza, Palestine

d Technology & applied Sciences, Al-Quds Open University, Gaza Branch, Gaza, Gaza Strip, Palestine

Abstract

Nanoparticles of undoped and cobalt-doped copper ferrite Cu1-xMnxFe2O4 (x= 0.2, 0.4, 0.6, 0.8 and 1.0) were successfully synthesized by a co-precipitation method. The existence of well-defined single cubic spinel structure was confirmed by X-ray diffraction in all the samples. The crystallite size found by XRD increased from ∼10.2 to∼20 nm. The lattice parameter increased from 8.332 to 8.371Å with increasing the Mn2+ content. The band gap energy of nanoferrites is found to decrease from 3.65 to 3. 20 eV with increase the content of Mn2+ ions. It has been observed that the luminescence intensity increases in copper ferrite matrices with increase the ratio of Mn2+. The saturation magnetization increases with increasing manganese ion concentration as indicated in the M-H loops.

## Keywords

Cu-Mn Ferrites; Magnetic; Nanoparticles; X-ray diffraction; Optical properties

----------------------------------------------------

*Corresponding author. Tel.: +9722876672; fax: +9722832180.

E-mail address: talaathammad@gmail.com(T.M.Hammad).