Nanofibrous Injectable and thermosensitive hydrogel for bone tissue engineering

Geeta Kumari Wasupalli 1, Devendra Verma

1 Department of Biotechnology and Medical Engineering, National Institute of Technology, Rourkela, Odisha 769008, India,

2 Department of Biotechnology and Medical Engineering, National Institute of Technology, Rourkela, Odisha 769008, India.

Keywords: Polyelectrolyte complexes (PECs), Chitosan,

Hydrogels, Thermogelation

At present, the use of injectable hydrogels is limited by the challenge of attaining quick gelation, excellent mechanical strength, and cytocompatibility. Polymeric self-assembly is a powerful tool to generate functional materials that combine multiple features and can respond to external factors. We have developed fiber-reinforced composite hydrogels in this study that display significantly increased mechanical strength, reduced gelling time, and excellent cytocompatibility. The feasibility of using self-assembled fibers of polyelectrolyte complex (PEC) with hydroxyapatite to develop a chitosan-based thermogelling solution was evaluated. By varying the concentration of βGP added to the chitosan solution, the effect of βGP concentration on gelation time was studied. Different combinations were screened to generate an appropriate hydrogel environment for cell encapsulation, development, and proliferation at physiological pH and temperature. Young modulus determination disclosed that hydrogel-reinforced PEC fibers were 2.5 times stiffer than chitosan-βGP gels. The gelation time was decreased to three minutes, and at physiological pH, temperature, the hydrogels had porous structures and gels and showed  > 80% viability of MG63 cells for MTT assay. Besides, PEC fiber-reinforced hydrogel confocal imaging showed noticeable viability and proliferation. FTIR was used to study the molecular interactions of gelling agents, polyelectrolytes, and hydroxyapatite. We researched interfacial bonding between βGP, NaHCO3, HAp, and PEC fibers. The combination of hydroxyapatite and polymer self-assembly technique has enhanced the feasibility of injectable hydrogels that help in minimally invasive applications.

Reference:

1	J. Fu, F. Yang, Z. Guo, The chitosan hydrogels: from structure to function, New J. Chem. 42 (2018) 17162–17180

- J.H. Lee, Injectable hydrogels delivering therapeutic agents for disease treatment and tissue engineering, Biomater. Res. 22 (2018) 1–14.

- G.K. Wasupalli, D. Verma, Molecular interactions in self-assembled nanostructures of chitosan-sodium alginate based polyelectrolyte complexes, Int. J. Biol. Macromol. 114 (2018) 10–17.

### Biography:

Wasupalli Geeta Kumari is a Ph.D. scholar in Biotechnology and Medical Engineering at National Institute of Technology, India, working under the supervision of Dr. Devendra Verma. Her research interest is in the development of polymeric scaffolds with high wet strength for bone tissue engineering. Her research interest includes bioinspired hydrogels, self-assembly biopolymers, biomaterials, and tissue engineering.

Full Name: Wasupalli Geeta Kumari                Contact number: 9439789760

Session name/ number: Oral session- Tissue Engineering

Category: Oral presentation

Passport Number:  R3574322