Novel, eco-friendly, and sustainable pyrometallurgical recycling techniques to transform waste Ni-MH batteries to value-based alloys

Behera PR*, Farzana R, Rajarao R, and Sahajwalla V

Centre for Sustainable Materials Research and Technology (SMaRT@UNSW),

School of Materials Science and Engineering, UNSW Sydney

NSW 2052, Australia

Keywords: Waste Ni-MH battery, e-waste plastic, hydrogen plasma, nickel-cobalt alloy, e-waste recycling, sustainability

- Abstract

Recovery of valuable metals such as nickel, and synthesis of alloys (Ni-Co and Fe-Ni) from waste Nickel-metal hydride (Ni-MH) batteries is a major area of focus and interest in this present work. Novel, green, and sustainable techniques, such as combination of two waste streams (e-waste plastics as a potential carbon source and waste Ni-MH batteries) and hydrogen plasma smelting are adopted to synthesize industry grade nickel-cobalt alloy and ferro-nickel alloy. Reduction of nickel oxide present in waste Ni-MH battery, using e-waste plastic, facilitated 99% nickel-cobalt alloy with ICP-OES and XPS analysis corroborating the results. Usage of e-waste plastic, as a potential alternative to conventional carbon, observes the gas-based reduction of nickel oxide. Hydrogen plasma smelting of nickel oxide in a maintained reducing ambience of argon and hydrogen flow rate (1:1) experiences the rapid reduction reaction (1800-2000°C), duly complemented by three forms of hydrogen (atomic, molecular, and ionic). The formation of ferro-nickel occurs within 15 min with Fe (66 wt%), Ni (31 wt %) and Co (2%) that are close to the industry standard. Moreover, hydrogen plasma smelting pushes rare earth elements (present in cathode of Ni-MH battery) to slag phase (La: 24 wt%, Ce: 11 wt%, and Nd: 7 wt%) without contaminating the product phase. Characterisation analysis of product and slag phase were performed using XRD, XPS, and SEM-EDS techniques. These scientific recovery techniques put forth a promising eco-friendly and sustainable solution to utilise waste resources in a befitting way, thus recovering valuable metals and alloys and safeguarding the environment at the same time.

- Image

- Reference

- Kuzuya, T., Hirai, S., Sokolov, V.V., 2013. Recovery of valuable metals from a spent nickel–metal hydride battery: Selective chlorination roasting of an anodic active material with CCl4 gas. Sep. Purif. Technol., 118: 823–827

- Heegn, H., Friedrich, B., Muller, T., Weyhe, R., 2003. Closed-loop recycling of nickel, cobalt and rare earth metals from spent nickel-metal hydride batteries. Proceedings of the XXII International Mineral Processing Congress. Cape town

- Muller, T., Friedrich, B., 2006. Development of a recycling process for nickel-metal hydride batteries. J. Power Sources, 158: 1498–1509

- Biography

Behera is pursuing his Ph.D. at SMaRT Centre in the school of Materials Science and Engineering, UNSW, Sydney, Australia. His research interests include high-temperature processing and recovery of waste Ni-MH batteries and other e-waste.

- Presenting author details

Full name: Pravas Ranjan Behera

Contact number: +61-416313105

Session name/ number: Track 11

Category: Oral presentation

Passport Number: K5000423