# Evaluation of the effect of the methodology of inclusion of oxygenated groups in activated carbon derived from rubber tires, on the performance and stability of iron catalysts supported in the Fenton oxidation of amoxicillin

González, Jenny.Ing, Universidad Nacional, Colombia.

Conde, Laura. PhD, Universidad Jorge Tadeo Lozano, Colombia.

Ramirez, Herney, PhD Universidad Nacional, Colombia.

### Abstract

Antibiotics generate resistance in pathogenic microorganisms making medical treatments for their elimination increasingly difficult (García Gómez, Gortáres Moroyoqui, and Drogui, 2011). In 2015, 42.3 billion daily doses of antibiotics were consumed worldwide (Klein et al., 2018), in the case of amoxicillin a broad-spectrum antibiotic, between 60 to 80% of the ingested amoxicillin eliminates through urine (facmed, 2018), ending in the waste waters. Supported iron catalysts were obtained, using rubber carbon-derived activated carbon as support, modified by the inclusion of oxygenated groups, to assess its effect on active phase stability and catalytic activity, during the degradation of amoxicillin by Fenton reaction. Activated carbon was obtained by physical activation of waste tire ruber with CO2, subsequently the modification of surface chemistry was performed by treatment at 473K with oxygen diluted (5% v/v) in nitrogen. Iron was supported through incipient wet impregnation, to achieve an iron load of 10% w/w in the catalysts. The supports were characterized by N2 adsorption isotherms at 77 K, X-ray diffraction (XRD) and Fourier transform infrared spectroscopy (FTIR), while the catalysts were characterized by XRD and FTIR. Fenton reactions were carried out at 25 °C, pH of 2, 80 mg H2O2/L and initial amoxicillin concentration of 100 mg/L; the degree of amoxicillin mineralization was stablished by total organic carbon analysis (TOC). The stability of the catalyst was evaluated throught quantification of iron in the final solution and on the catalyst before and after the reaction, by atomic absorption.

Recent Publications

- Abdelouahab Reddam, Z. (2015). Catalizadores soportados en carbón activado para la oxidación total de Compuestos Orgánicos Volátiles. Taller Digital, 227.

- Acevedo, S., Giraldo, L., & Carlos Moreno-Piraján, J. (2017). Caracterización de carbones activados modificados con agentes quelantes para la adsorción de metales tóxicos en solución acuosa. Afinidad LXXIV, 578(June), 101–107.

- Alalm, M., Tawfik, A., & Ookawara, S. (2014). Degradation of four pharmaceuticals by solar photo-Fenton process : Kinetics and costs estimation. Journal of Environmental Chemical Engineering, 3(1), 46–51. http://doi.org/10.1016/j.jece.2014.12.009

- Alaton, I. A., Dogruel, S., Baykal, E., & Gerone, G. (2004). Combined chemical and biological oxidation of penicillin formulation effluent. Journal of Environmental Management, 73(73), 155–163. http://doi.org/10.1016/j.jenvman.2004.06.007

- Ampar, A. C., Gonz, G., Robau, A., & Casarrubias, L. B. (2007). Modificación con hierro de carbón activado para remover As en agua Modificación con hierro de carbón activado para remover As en agua.

- Ay, F., & Kargi, F. (2010). Advanced oxidation of amoxicillin by Fenton’s reagent treatment. Journal of Hazardous Materials, 179(1–3), 622–627. http://doi.org/10.1016/j.jhazmat.2010.03.048

- Baquero, F., Martínez, J.-L., & Cantón, R. (2008). Antibiotics and antibiotic resistance in water environments. Current Opinion in Biotechnology, 19, 260–265. http://doi.org/10.1016/j.copbio.2008.05.006

- Barroso, A. (2010). Catalizadores de Hierro soportado sobre carbón activado para la oxidación catalítica de fenol con peróxido de hidrógeno. Instituto de Catálisis y Petroleoquímica. Universidad Autónoma de madrid Facultad de ciencias.

- Castro, G. (2008). Materiales y compuestos para la industria del neumatico. Facultad de Ingeniería Universidad de Buenos Aires.

- Catalá, M., Domínguez-Morueco, N., Migens, A., Molina, R., Martínez, F., Valcárcel, Y., … Segura, Y. (2015). Elimination of drugs of abuse and their toxicity from natural waters by photo-Fenton treatment. Science of the Total Environment, 520, 198–205. http://doi.org/10.1016/j.scitotenv.2015.03.042

- http://www.facmed.unam.mx/bmnd/gi_2k8/prods/PRODS/15.HTM

- Fernandez, C. (2014). El humo negro de la quema de llantas causa daños a la salud - Archivo Digital de Noticias de Colombia y el Mundo desde 1.990. Retrieved October 9, 2018, from https://www.eltiempo.com/archivo/documento/CMS-14798935

- Fernández, C. (2015). Síntesis, caracterización y actividad catalítica de zeolitas de tamaño de poro medio en la reacción de reducción de NOx. Universidad poltecnica de valencia. Univerisdad Politécnica de Valencia.

- Figueiredo, J. L. (2013). Functionalization of porous carbons for catalytic applications. Materials Chemistry A, (207890), 32

- Figueiredo, J. L., Pereira, M. F. R., Freitas, M. M. A., & Orfao, J. J. M. (1999). Modification of the surface chemistry of activated carbons. Carbon, 37, 1379–1389.

- García Gómez, C., Gortáres Moroyoqui, P., & Drogui, P. (2011). Contaminantes emergentes : efectos y tratamientos de remoción. Revista Química Viva, (2), 96–105.

- Klein, E. Y., Van Boeckel, T. P., Martinez, E. M., Pant, S., Gandra, S., Levin, S. A.,… Laxminarayan, R. (2018). Global increase and geographic convergence in antibiotic consumption between 2000 and 2015. Proceedings of the National Academy of Sciences of the United States of America, 115(15), E3463–E3470. https://doi.org/10.1073/pnas.1717295115

Biography

Jenny González has her expertise in development of porous materials and passion for waste management, She has been using waste tires where they are transformed into useful products like activated carbon and catalysts for wastewater treatment and removal of contaminants in water such an emerging contaminants  pesticides and pharmaceuticals. She has been exploring different alternatives for taking advantage waste tire that is the important environment problem, for the amount that is discarded in the world.

Email: jegonzalezz@unal.edu.co

Notes/Comments: