## Slide 1
Sustainability through Catalysis: Making Fuels and Chemicals from Biomass
Mahdi Abu-Omar Department of Chemistry
and School of Chemical Engineering

## Slide 2
A Barrel of Oil
Chart: 
http://www.evecosolutions.co.uk/biomass-boiler.html
Energy Information Administration, “Oil: Crude Oil and Petroleum Products Explained” and Annual Energy Outlook 2009 (Updated February 2010).

## Slide 3
Moving towards sustainability
Chart: 
Zakzeski et al Chem. Rev. 2010, 110, 3552-3599.

## Slide 4
Chart: 
| 1st Qtr | 2nd Qtr | 3re Qtr
Transportation Primary Energy Source | 73 | 7 | 23
Biomass availability potential = 498 Million metric tons/yr
Liquid fuel use in the USA, 2013 =12.75 Mbbl/day
Stand alone Biomass
Petroleum
Natural Gas
Biomass
Other
Integration
~30% of transportation by integrated process with 63% GHG emission reduction and ~2 tcf NG
δng=10%
Chart: 
| 1st Qtr | 2nd Qtr | 3re Qtr | 4th Qtr
Transportation Primary Energy Source | 64.6 | 7 | 28.4
Emre Gencer and Rakesh Agrawal
Process Integration

## Slide 5
Lignin: Rich in energy but underutilized
Lignin accounts for 37% of the carbon in biomass
Chart: 
Linkage Types
β-O-4
5-5
α-O-4
β-5
8-8

## Slide 6
Catalytic depolymerization and HDO
Chart: 
5% wt. Zn-Pd/C
300 psi H2
150 °C, MeOH
165 [M-H]-
181 [M-H]-
Abu-Omar et al. Chem. Sci. 2013, 4, 806-813.
A
C
B
ISTD
195 [M-H]-
A
B
C

## Slide 7
Catalyst characterization
Pd K-edge Fourier transform XAS
0.0
0.02
0.04
0.0
-0.02
-0.04
0
1
2
3
4
R [Å]
FT[k2 * Chi(k)]
Pd Foil
Zn/Pd/C Catalyst
Pd NP 3-4 nm
Abu-Omar et al. Chem. Sci. 2013, 4, 806-813.

## Slide 8
Catalytic depolymerization of native lignin
5 wt% Cat.
30 bar H2, 200 °C
1-20 g biomass
Yield 54%
Time/ min
Intensity
Abu-Omar et al. Green Chem. 2015, 17, 1492-1499.
(Highlighted in Science 2015, 347, 1111.)
Wild Type Poplar

## Slide 9
Carbohydrate residue is intact
Sugars
Gasoline
85-95%
Ethanol

## Slide 10
Platform chemicals
Fufurals and levulinic acid
• Iron is earth abundant and cheap.
• Lewis and Brønsted acid.

## Slide 11
Reaction conditions
Glucose, fructose, or HMF = 0.25-1.00 M
FeCl3(H2O)6, Fe2(SO4)3, or Fe(SO4) = 0.01-0.10 M
Water (monophasic) or Water:Me-THF (biphasic)
Microwave heating or conventional (140 °C)
Quench periodically and analyze by HPLC & 1H NMR (organic phase)
23

## Slide 12
Speciation of iron confirmed
UV-vis
Operando XANES

## Slide 13
Kinetics: HMF to LA
k3 = 0.48 x 10-3 s-1
k4 = 0.23 x 10-3 s-1
@ pH = 1.1 and [Fe] = 0.10 M

## Slide 14
Kinetics: Fructose
k2 = 2.2 x 10-3 s-1
k5 = 1.0 x 10-3 s-1
k3 = 0.48 x 10-3 s-1
k4 = 0.23 x 10-3 s-1
@ pH = 1.1 and [Fe] = 0.10 M

## Slide 15
Kinetics: Fructose
k1 = 0.053 x 10-3 s-1
k2 = 2.2 x 10-3 s-1
k5 = 1.0 x 10-3 s-1
k3 = 0.48 x 10-3 s-1
k4 = 0.23 x 10-3 s-1
@ pH = 1.1 and [Fe] = 0.10 M

## Slide 16
Lewis versus Brønsted acid catalysis
H3O+
H3O+
Abu-Omar et al, Org. Chem. Front. 2015, 2, 1388 - 1396.

## Slide 17
Monophasic versus biphasic
Effect of Me-THF solvent
Observed rate const. (x103)/ s-1 | k2 | k3 | k4 | k5
Water | 2.2 | 0.48 | 0.23 | 1.0
Water:Me-THF | 3.3 | 0.07 | 0.06 | 0.065
@ pH = 1.1 and [Fe] = 0.10

## Slide 18
Cellulose
Solid
Residue
HDO
Depolymerization
Dehydration
Utilization of the Entire Biomass

## Slide 19
Research scientist
  Dr. Basudeb Saha
Postdoc
  Dr. Trenton Parsell
Graduate Students
  Dr. Ian Kelin (Ph.D. 2015)
  Dr. Christine Bohn (Ph.D. 2014)
  Yuan Jiang
  Hao Luo
$upport
  C3Bio, EFRC, U.S. Department of Energy, Office of Science, Award no. DE-SC0000997
  Spero Energy, Inc.
Collaborators
  Nate Mosier (Purdue University)
  Hilkka Kenttämaa (Purdue University)
  Clint Chapple (Purdue University)
  Rick Mielan (Purdue University)
  Fabio Ribeiro (Purdue University)
  Rakesh Agrawal (Purdue University)
  Jeffrey Miller (Purdue/ANL)
Acknowledgment
Notes: 19
19