## Slide 1: Thermo-chemical pretreatments for the combined recovery of extractives and bioethanol production from softwood bark C. Sambusiti, Chloé Navas, Eric Dubreucq, Abdellatif Barakat
Past and Present Research Systems of Green Chemistry
September 14-16/2015 Orlando (USA)

## Slide 2
Introduction – Lignocellulosic biorefinery (2° generation)
BIOMASS
Biological platforms
Thermochemical platforms
Renewable energies
(CHP system)
Fuels, chemicals & materials
Anaerobic digestion
Dark fermentation
Bioethanol fermentation
Oil extraction
Bio-diesel
BioCH4
BioEtOH
BioH2
Combustion
Pyrolysis
Gasification
HTC & HTL
VFA

## Slide 3
Lignocellulosic biomass – structure/composition
Scheme of composition of plant cell walls in a lignocellulosic matrix. (adapted from Monlau et al., 2012).
Cellulosic structures are interconnected by a network of hemicelluloses embedded by lignin.
Cellulose : 10-60%
Hemicelluloses: 10-40%
Lignin: 5-60%

## Slide 4
Lignocellulosic pretreatments - categories
Physical
Mechanical (i.e. chipping, grinding, milling, …)
Steam explosion, Liquid Hot Water
Microwaves,
Ultrasound
Chemical
Enzymes or fungi
Ensiling
Oxidative, alkaline, dilute-acid, ionic liquids, wet oxidation and inorganic salts pretreatments
Biological
 | Pretreatments | Mechanical | Chemical | Physicochemical | Biological
Physico-chemical properties | Particles size | ●●● | ○ | ○ | ○
 | Specific surface area (SA) | ●●● | ●● | ● | ●
 | Polymerization degree | ●● | ●●● | ●● | ●●●
 | Pore volume | ●● | ●● | ● | ●
 | Crystallinity (CrI) | ●●● | ●● | ● | ○
 | Lignin solubilisation (LiG) | ○ | ●● | ● | ●●
 | Hemicelluloses solubilisation | ○ | ●●● | ●● | ●●
 | LCCs degradation | nd | ●● | nd | nd
 | Cellulose solubilisation | ○ | ●● | ● | ●●
●●● major positive effect, ● minor positive effect, ○ No effect

## Slide 5
Lignocellulosic pretreatments - drawbacks
F. Monlau , C. Sambusiti, A. Barakat, M. Quéméneur, E. Trably, J.-P. Steyer, H. Carrère (2014). Do furanic and phenolic compounds of lignocellulosic and algae biomass hydrolyzate inhibit anaerobic mixed cultures? A comprehensive review. Biotechnology Advance.

## Slide 6
Pretreatments:
Mechanical (chipping, milling,....)
Physico-chemical (steam explosion,...)
Enzymatic hydrolysis
Fermentation
SHF
SSF
De-barked
Barked
Ethanol
Introduction – Softwood-to-ethanol process scheme

## Slide 7
 | Wood | Bark
Lignin (%)* | 25-30 | 40-55
Polysaccharides (i.e. glucan, mannan, xylan, galactan, arabinan) (%)* | 66-72 | 30-48
Extractives (%) | 2-9 | 2-25
Ash (%)* | 0.2-0.6 | Up to 20
N.B. Chemical composition varies according to plant type, plant varieties, plant part and maturity
BARK
(INNER AND OUTER)
WOOD
* Based on extractives free material (USDA et al., 1971)
Introduction – Chemical composition of softwoods
≈ 12% of the total weight of a tree

## Slide 8
Group of non-structural components in wood
They consist of both hydrophilic and lipophilic compounds
Dissolves in either water or organic solvents
Protects the tree from microbic and insect attacks
Different amounts and distribution of extractives, dependent on: - wood species - growing site (latitude, altitude, wind exposure etc) - position within the tree - genetic factors
Introduction – Extractives
Oleoresins (i.e. monoterpenoids and diterpenoids)
R1= fatty acid chain
Waxes
Phenolic compounds
1. Stilbenes
3. Lignans
4. Flavanoids
2. Tannins
Fatty acids

## Slide 9
Objectives of this work
Evaluation of the effect of organosolv/diluted acid pretreatment on chemical composition of softwood bark
Evaluate the feasibility of ethanol production from softwood bark and the influence of residual extractives on ethanol fermentation

## Slide 10
Materials and methods – experimental procedure
Softwood bark
Liquid fraction
Solid fraction
Cutting milling
(2 mm screen size)
Organosolv/diluted acid
pretreatment
Simultaneous Saccharification and Fermentation (SSF)
Extractives

## Slide 11
Materials and methods – pretreatment conditions
 | Organosolv | Diluted acid | Diluted acid-Organosolv
Solid loading (gTS.L-1) | 100 | 100 | 100
H2SO4 dosage (mM) | - | 8 | 8
Ethanol dosage (% v/v) | 65 | - | 65
Temperature (°C) | 150-180 | 150-180 | 150-180
Time (h) | 1 | 1 | 1

## Slide 12
Materials and methods – Ethanol fermentation
Operational conditions:
T° = 40°C,
Time = 72 h
pH = 5
Stirring: 500 rpm
Test preparation:
Solid loading: 60 gTS/L
Enzymatic cocktail: xylanase (33.15 IU/gTS), endoglucanase (261 IU/gTS), exoglucanase (1.14 IU/gTS) and beta-glucosidase (4785 IU/gTS)
Nutritive solution: acetate buffer (50 mM, pH=5); yeast extract (5 g/kg); urea (0.4 g/kg); 50 ppm chloramphenicol)
Yeast: S. cerevisiae for C6 conversion, produced by our team (1.5 g/kg)
Monomeric sugars and ethanol analysed by HPLC

## Slide 13
Results – chemical composition
Parameter | Mean±S.D.
TS (gTS.100g-1fresh matter) | 94.6 ± 0.0
VS (gVS.100g-1TS) | 97.7 ± 0.1
Ash (g.100g-1TS) | 2.1 ± 0.2
Cellulose (g.100g-1TS) | 14.9± 2.3
Hemicelluloses (g.100g-1TS)* | 10.3 ± 1.7
Klason lignin (g.100g-1TS)** | 60.4 ± 2.1
DCM extractives (g.100g-1TS) | 9.8 ± 1.5
Proteins (g.100g-1TS) | 2.4 ± 0.3
* Xylose/mannose/galactose/arabinose monomers
**Calculated after extraction with DCM
Untreated softwood bark

## Slide 14
Results – chemical composition
Molecule Structure | Chemical formula | Extract DCM mg/gTS
Polyols |  | 
(Z)-4-methyl-pent-2-ene-2,4-diol | C6H12O2 | 45.81
Fatty acids and other carboxylic acids |  | 
palmitic acid | C16H32O2 | 21.02
oleic acid | C18H34O2 | 5.78
Aromatic compounds |  | 
2-(3,4-dihydroxyphenyl)chroman-3,5,7-triol | C14H8O4 | 6.69
Resin acids |  | 
isopimaric acid | C20H30O2 | 4.46
dehydroabietic acid | C20H28O2 | 12.87
Alkaloids |  | 
agroclavine | C16H18N2 | 2.74
Untreated softwood bark

## Slide 15
Chart: Chemical composition (g./100gTSin)
| Untreated | Organosolv 150°C | Organosolv 180°C | Diluted acid 150°C | Diluted acid 180°C | Diluted acid-organosolv 150°C | Diluted acid-organosolv 180°C
Cellulose | 14.9067 | 14.3737 | 13.0585 | 13.7489 | 12.7893 | 12.5171 | 13.1616
Hemicelluloses | 10.2789 | 10.7741 | 9.2856 | 8.8841 | 6.1974 | 10.1841 | 8.6613
Klason lignin | 60.3794 | 47.1484 | 49.5716 | 57.4512 | 58.6507 | 50.1815 | 47.6898
Results – chemical composition
Pretreated softwood bark (solid separated residues)

## Slide 16
Results – chemical composition
Exctractives recovery after pretreatment (liquid fractions)
 | Organosolv |  | Diluted acid |  | Diluted acid-organosolv | 
 | 150 °C | 180 °C | 150 °C | 180 °C | 150 °C | 180 °C
 | mg g-1TSin |  |  |  |  | 
Polyols | 11.1 | 4.2 | 0.4 | 0.4 | 6.2 | 5.6
Fatty acids and other carboxylic acids | 7.3 | 6.1 | 0.2 | 0.6 | 3.5 | 2.7
Sugar derivatives | 5.3 | 11.7 | 0.1 | n.d. | 4.5 | 12.9
Aromatic compounds | 8.6 | 7.3 | 0.2 | 0.8 | 11.6 | 5.4
Resin acids | 7.6 | 4.2 | n.d. | n.d. | 3.6 | 2.8
Total | 39.9 | 33.6 | 0.9 | 1.8 | 29.3 | 29.3

## Slide 17
Results – Simultaneous saccharification and fermentation
yeast quickly consumed free glucose after inoculation and more than 90% of the ethanol was produced during the first 48h in all fermentations.
Fermentation of untreated bark produced 12 g/kgTS (16% of the theoretical conversion of glucose).
Organosolv pretreatment performed at 150°C led to the highest increase of ethanol yield (up to 20 g/kgTS), corresponding to 18% of the theoretical conversion of glucose.
Ethanol yields are very low confirming that during SSF enzymatic hydrolysis of cellulose is the limiting step.

## Slide 18
Conclusions
In terms of chemical composition:
All pretreatments led to a solubilization of lignin, tannins and suberin
Cellulose was not solubilized by the pretreatment, while a slight solubilization of hemicelluloses seemed to occur also during organosolv and diluted acid pretreatments, especially at 180°C.
The amount of extractives originally present in the untreated bark, were not totally solubilized by the pretreatments. However, organosolv and diluted-acid organosolv pretreatments led to a high release of extractives (up to 40% w/w) if compared to those originally present in the bark sample.
According to fermentation results:
In all cases the yeast quickly consumed free glucose after inoculation during the first 48h in all fermentations. These results suggest that no inhibition of fermentation occurred during SSF
Experimental ethanol yields are very low compared to the expected, so enzymatic hydrolysis of cellulose remains the limiting step.

## Slide 19
Acknowledgment
This research study has been supported by FUTUROL project , which is gratefully acknowledged.
The authors are also grateful to BPI-France for the financial support to the project.

## Slide 20
Thanks for your attention!