## Slide 1
Green Fuel: Selective and Water Compatible Catalysts for Solar Fuel Production
Hongjin Lv, Ben Yin, Yurii V. Geletii, James W. Vickers, Sarah M. Lauinger, Tianquan Lian, Djamaladdin G. Musaev, John Bacsa, Paul Kögerler, Craig L. Hill
Department of Chemistry
Emory University, Atlanta, GA, USA
Funding:
U.S. DOE, Basic Energy Sciences & NSF

## Slide 2
• Rate
• Stability (particularly WOCs)
• Selectivity (WOCs, CO2 reduction catalysts)
Challenges for Solar Fuels Catalysts
• Photoelectrode – catalyst interface
• WOCs (OECs) effective at very low pH
• Catalyst counterions impact all the above.
• Catalyst behavior: solution vs. immobilized
• Earth abundant elements; facile and green processing
• Inhibit photocorrosion
immobilization techniques for molecular catalysts
effective spectroscopic and diffraction probes of monolayer coverages

## Slide 3
• Idea: -- use POMs as catalysts (first, WOCs): they combine the advantanges of both without the disadvantages of both.
Multi-electron catalysts (WOCs, WRCs, CO2-RCs)
Heterogeneous (NPs, films, etc.)
More stable, lower cost, manufacturable at scale
BUT !
Unstable (hydrolytically, oxidatively and thermally)
BUT !
Extremely hard to study and understand at molecular level
Progress toward viable catalysts
Homogeneous / molecular
Can be studied experimentally and theoretically, thus optimized and formulated
• Two communities – little overlap; need to converge

## Slide 4
Polyoxometalates (POMs):
early-transition-metal oxygen anion clusters
n [WO4]2- [WxOy]n- + nH2O WO3 + nH2O
H+
OH-
metal oxide
H+
OH-
polyoxometalates
[AlW12O40]6- (Keggin)
Al, purple; W, gray, O, red
• stable (O2, H2O)
• accessible
• scalable
• nontoxic
• inexpensive
readily alter:
• elemental compositions
• potentials
• acidities
• solubilities
• shape, size, charge
• others
• counterions
Excellent oxidation catalysts AND corrosion inhibitors

## Slide 5
[{Ru4O4(-XW10O36)2]10-
Ru4POM, X = Si or P
ACIE 2008, 47, 3896
JACS, 2009, etc.
TOF ~ 1 sec-1
Polyoxometalate (POM) Water Oxidation Catalysts (WOCs)
[Ni5(Si2W18O66)]10-
Ni5POM
Dalton, 2012,
41, 13043
JACS, 2014, 136, 9268
[Co4(α-VW9O34)2]10-
Co4V2
~ 6 sec-1
~ 10 sec-1
~ 1000 sec-1
Science, 2010, 328, 342;
JACS, 2011, etc.
[Co4(α-PW9O34)2]10-
Co4P2
TOFs depend on many parameters. Reporting TOFs for light-driven WOCs can be tricky.

## Slide 6
Co4P2 Hill group (Science, 2010), then challenged by Finke, Scandola-Bonchio, but confirmed homogeneous catalyst by H. Dau, J.R. Galán-Mascarós, R. Finke, M. Nyman (just published).
Mn4O4(L)4 Original work (homo cat) clarified as heterogeneous catalyst precursor -- Spiccia et al. Nature Chem, 2011
Co4O4(OAc)4(pyr)4 Original work (homogeneous cluster) clarified as Co2+ -- Nocera et al. JACS, 2014.
NiOOH Original work (heterogeneous WOC) but Fe impurities are critical to activity – Boettcher et al. JACS, 2014.
Others
Multielectron catalysts in H2O –
homogeneous or heterogeneous?
Clarification of initial reports:

## Slide 7
Many methods:
spectra (IR, NMR, etc. before and after catalysis)
rate laws (pH dependence)
DLS
SAXS
controls (e.g. activity of CoOx)
recovery/reuse (initial kinetics for H2O oxidation)
electro-catalytic activity (e.g. [Ru(bpy)3]2+ oxidation)
bpy present scavenges all Co2+ and prevents CoOx.
electrochemical quartz crystal nanobalance -- Crabtree, Brudvig
extraction of POM (not Co2+ or CoOx) into organic solvent
Homogeneous vs. heterogeneous catalyst(s) in H2O?
Vickers, J. W.; Lv, H.; Sumliner, J. M.; Zhu, G.; Luo, Z.; Musaev, D. G.; Geletii, Y. V.; Hill, C. L. J. Am. Chem. Soc., 2013, 135, 14110.

## Slide 8
Quantification of catalytic water oxidation by:
Co4P2 vs. Co2+(aq) vs. CoOx
NaPi
NaB
CAdSV
0.54 ± 0.04 µM
0.07 ± 0.01 µM
ICP-MS
0.44± 0.02 µM
0.07 ± 0.01 µM
Co2+, CoOx extract 0%
Should be general method for assessing soluble and insoluble WOCs
POM (red) extracts 100% from H2O into
toluene phase containing R4N+
H2O
toluene
Vickers, J.W. et al. J. Am. Chem. Soc., 2013, 135, 14110−14118

## Slide 9
Comprehensive study of Co4P2:
reactivity and stability
Vickers, J. W.; Lv, H.; Sumliner, J. M.; Zhu, G.; Luo, Z.; Musaev, D. G.; Geletii, Y. V.; Hill, C. L. J. Am. Chem. Soc., 2013, 135, 14110.

## Slide 10
Photocatalytic Water Splitting Cells – Catalysts Immobilized
Immobilization of POMs on photoelectrode surfaces
3 ways:
• electrostatic (usually easy and effective)
• hydrophobic (usually easy; POM hydrolytically stabilized
but organic groups can oxidize)
• covalent (easy for many types of POMs, but not yet for
POM WOCs, WRCs, etc.)

## Slide 11
TiO2-P2-Ru4POM Triadic Photonodes
Conditions:
Ref. electrode: Ag/AgCl,
3 M NaCl
Electrolyte: 3~5 mM
Na2SiF6-NaHCO3
pH 5.8
0 V (vs Ag/AgCl), +0.56 V (RHE)
Illumination: 420 to 470 nm
Our group: X. Xiang, J. Fielden et al. J. Phys. Chem. C 2013, 117, 918−926
F. Scandola, M. Bonchio et al., Chem. Commun. 2010, 46, 3152

## Slide 12
-
aqueous
POM
rt
TiO2, BiVO4
~ 1 - 1.5 nm
3-aminopropyltrimethoxysilane
(APS)
Electrostatic POM immobilization can be improved by metal oxide (MOx) silylation with cation
Ru4POM Ru4POM-TiO2-APS
MOx
+
+
+
+
NH3+
POM
-
POM
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
pH < 10
toluene
rt
MOx
MOx
Sarah Lauinger
Idea: have enough catalyst on surface in monolayer to quantify it.
Notes: First, the methoxy groups of the silane coupling reagent reacted cleanly with the hydroxyl groups of TiO2 to eliminate MeOH resulting in the formation of isolated surface species.
pKa RNH3+=10.66
The grafted PMoV can be removed by the addition of tetrabutylammonium bromide (TBABr) to form TBA4[PMo11VVO40], suggesting that there is no covalent bonding between the vanadium site and the ammonium groups.

## Slide 13
I-V curve
Hydrophobic R4N+ immobilizes and stabilizes POMs in carbon paste electrodes
Conditions: 20 wt % TBA-Co4V2 in carbon paste, 80 mM pH 8.0 NaBi buffer, 0.2 M NaClO4 as supporting electrolyte, 100 mV/s.
Electrocatalytic curve where λ and γ are high;
λ = (RT/nF)/(keCP0/ν)
γ = (CA0/CP0)
i.e. where there is competition between rate-limiting substrate (H2O) consumption and diffusion.

## Slide 14
I-V curve
Hydrophobic R4N+ immobilizes and stabilizes POMs in carbon paste electrodes
Conditions: 20 wt % TBA-Co4V2 in carbon paste, 80 mM pH 8.0 NaBi buffer, 0.2 M NaClO4 as supporting electrolyte, 100 mV/s.
FTIR of TBA-Co2V2
Hongjin Lv

## Slide 15
I-V curve
Hydrophobic R4N+ immobilizes and stabilizes POMs in carbon paste electrodes
O2 also now quantified. See system for fast monitoring of spectra and O2: Vickers, Sumliner, Lv, Morris, Geletii, Hill, PCCP, 2014, 16, 11942.
FTIR of TBA-Co2V2

## Slide 16
TiO2-P2-Ru4POM Triadic Anodes: Catalytic photocurrent
Near 100% photocurrent enhancement
No photocurrent increase in MeCN, nor with catalytically inactive Zn4POM
Over 20 minutes: 40% loss of dye/catalyst absorbance for P2 system, due to desorption (not WOC damage)
J. Phys. Chem. C 2013, 117, 918

## Slide 17
Ru4POM transfers electron to photogenerated RuIIIP2 hole
TiO2-P2-Ru4POM Triadic Anodes:
Comparison of different oxides
J. Phys. Chem. C 2013, 117, 918
Chem. Science 2015, in press

## Slide 18: Hill group (April, 2015)
Missing: Emory collaborators: Jamal Musaev, Tim Lian, Paul Kögerler, Anil Mehta, Brian Dyer. Also John Fielden (now UEA).
Marika Wieliczko
Sarah Lauinger
Ben Yin
Yurii
Geletii
Hongjin
Lv
James
Vickers

## Slide 19
Ru4POM to dye electron transfer much faster than IrO2 to dye
Able to outcompete recombination
Computational modeling
Mallouk, Moore, Gust et al.
J. Am. Chem. Soc. 2009, 131, 926
Our work: J. Phys. Chem. C 2013, 117, 918
TiO2-P2-Ru4POM Triadic Anodes: Comparison with IrO2

## Slide 20
Photoelectrocatalytic H2O Oxidation by BiVO4-Ru4POM
Conditions
0.2 M pH 7.2 phosphate buffer
Xenon lamp (λ > 400 nm) at 80 mW/cm2
10 mV/s scan rate
Ref. vs Ag/AgCl in 1M KCl
Ben Yin

## Slide 21
Photoelectrocatalytic BiVO4-Ru4POM oxidation:
Sulfite versus H2O
Conditions
0.2 M pH 7.2 phosphate buffer
Xenon lamp (λ > 400 nm) at 80 mW/cm2
10 mV/s scan rate
Ref. vs Ag/AgCl in 1M KCl

## Slide 22
Photoelectrocatalytic BiVO4-Ru4POM oxidation:
Sulfite versus H2O
Conditions
0.2 M pH 7.2 phosphate buffer
Xenon lamp (λ > 400 nm) at 80 mW/cm2
10 mV/s scan rate
Ref. vs Ag/AgCl in 1M KCl
O2 also now measured.
See Vickers, Sumliner, Lv, Morris, Geletii, Hill, PCCP, 2014, 16, 11942.

## Slide 23
Conditions
0.2 M pH 7.2 phosphate buffer
Pt counter electrode
Xenon lamp (λ > 400 nm) at 80 mW/cm2
8 hours electrolysis at 0.66 V vs. RHE
Ref. vs Ag/AgCl in 1M KCl
Stability:
Photoelectrocatalytic H2O oxidation by BiVO4-Ru4POM

## Slide 24
Conditions
0.2 M pH 7.2 phosphate buffer
Pt counter electrode
Xenon lamp (λ > 400 nm) at 80 mW/cm2
Before and after 8 hours electrolysis at 0.66 V vs. RHE
Ref. vs Ag/AgCl in 1M KCl
Stability of BiVO4-Ru4-POM by Confocal Raman

## Slide 25
Ru4POM potentials (PCET, CCET events) easily quantified
DC CVs of 0.7 mM Rb8K2Ru4POM in 0.1 M aqueous HCl with (red) and without (black) 0.5 M KCl
J. Zhang, S-X Guo, J. Zhang, A. Bond, Y. Geletii, Inorg. Chem. 2012, 51, 11521 and Inorg. Chem. 2013, 52, 11986

## Slide 26
Ru4POM potentials (PCET, CCET) easily quantified
FT ac cyclic voltammetric fundamental (a) to eighth (h) harmonic components for RuIV/V oxidation (A/A´, B/B´) and RuIV/III reduction (C/C´, D/D´, E/E´, F/F´). WE = GC, 0.7 mM Rb8K2Ru4POM in 0.1 M aqueous HCl with and w/o 0.5 M KCl. Red = simulations
J. Zhang, S-X Guo, J. Zhang, A. Bond, Y. Geletii, Inorg. Chem. 2012, 51, 11521 and Inorg. Chem. 2013, 52, 11986

## Slide 27
In contrast:
potentials of 3d-metal POMs not easily measured.
Co4P2 & Co4V2 unstable at high anode potentials. Oxidation potentials not
accessible by CV.
Method that works: potentiometric titration of Co4P2 with [CoIIIW12O40]
1 mL of 2 mM [CoIIIW12O40] was titrated by 2 mM Co4P2 in 80 mM sodium borate buffer pH 8.0.
E1o and E2o both ~ 1.1 V where E1o = [Co4P2(I)] / [Co4P2(0)]
E3o and E4o both ~ 1.2 V vs. Ag/AgCl
Yurii Gueletii (Geletii)

## Slide 28
Counter cation effects on POM properties, catalysis and electrode surface immobilization
Largely ignored to date, but important in H2O ox, H2O red, CO2 red, and chemistry of the interface
First experiments: alkali metal salts of Ru4POM (10-)
(5 experiments quantify differences in Na+, Li+ versus K+)
Yurii Gueletii (Geletii)

## Slide 29
Counter cation effect #1: Kinetics of Ru4POM oxidation
by [Ru(bpy)3]3+ (stopped flow)
~1.0 mM [Ru(bpy)3]3+, 5 μM Ru4POM, 80 mM NaPi buffer, pH 7.0

## Slide 30
Effect of cations on the reversible potential (E0') for the Ru4POM (4445)/(4444) couple. 1M KNO3, NaNO3, LiNO3, 10 mM of Ca(NO3)2, 1M Mg(NO3)2, MgSO4 or Na2SO4. Britton-Robinson buffer (phosphate/acetate/borate)
Counter cation effect #2: Impact on POM potentials

## Slide 31
Titration curves of Ru4POM (oxidation state: 4444) in the presence of different electrolytes
Counter cation effect #3: pKa values

## Slide 32
Effects of pH and cations (at pH 2.0) on UV-vis spectra of Ru4POM
Ru4POM + H+ = Ru4POMH+ pKa
Ru4POM + K+ = Ru4POMK+ pKK
Ru4POMK+ + H+ = Ru4POMK+H+ pKaK
Counter cation effect #4: Impact on UV-vis spectra

## Slide 33: Counter cation effect #5: X-ray crystal structures (cation—O(POM distances) & K2Rb8 counterions located
Unusual interaction of K+ ion observed: K+ (“K2”) interacts directly with terminal aqua ligand on Ru.
Guibo Zhu, John Bacsa, Marika Wieliczko

## Slide 34: K2Rb8 versus K10{Ru4POM} crystal structures
Ru oxidation state confirmed by valence bond sum calculation + titration with [Ce(IV)]
Marika Wieliczko
Notes: In other words, O2 evolution via a RuV-toRuIII redox process does not appear to be feasible, but it does appear to be so via a RuVI-to-RuIV redox process in this Ru2 “monomer”, [{RuIII2(OH)2(H2O)2}(g-SiW10O36)]4- (which is half of 1) and 1 itself

## Slide 35
Findings
• Polyoxometalate (POM) catalysts: address rate, stability, selectivity + control of interface (PCET). Photocorrosion inhibition?
• POM WOC stability and reactivity better understood
• Quantifying homogeneous vs. heterogeneous catalysts simultaneously
• Photocatalytic POM-based dyads, triads
POM immobilization;
Many processes, understandable at molecular level, can be probed.
• POM-based chromophores and photosensitizers (PS)
• POM H2O, CO2 reduction catalysts (noble-metal-free and
water compatible, molecular -- J. Am. Chem. Soc. 2014, 136, 14015)
• pH 14-compatible POM WOCs
• Counter cation effects on POM physicochemical properties, catalysis, immobilization, interface dynamics

## Slide 36
End

## Slide 37: Potassium: Non-innocent Cation Interactions

## Slide 38
Three other research groups confirm our work: Co4P2 is the dominant WOC
Stracke, Finke ACS Catal., 2014, 4, 79
Limberg, Dau et al. Chem. Commun., 2014, 50, 100.
XAS: Co4P2 intact and
No catalytic cobalt oxide forms
Galan-Mascaros et al: 2 recent thorough papers:
Inorg. Chem. 2012, 51, 11707
Inorg. Chem. 2013, 52, 4753

## Slide 39
Need breakthroughs in fundamental science (not just engineering)
2 H2O + h (sun)  O2 + 2 H2
CO2 + 2 H2O + h (sun)  CH3OH + O2
Sunlight for energy
(hydroelectric, wind, tides, biofuel, geothermal, etc. aren’t sufficient)
Water as electron source
High density energy, hence “solar fuels”
Ultimately need:

## Slide 40
Approaches to solar fuels
Electron-donor-acceptor (EDA) and photoelectrochemical (PEC) systems
All systems:
(1) light absorption – charge separation
(2) catalytic H2O or CO2 reduction
(3) catalytic water oxidation
sunlight
H2O, CO2
H2, CH3OH
2 H2O
O2 + 4H+
- +
e-
e-
reduction catalyst(s)
A D
water oxidation catalyst (WOC)
antenna
(4) All 3 units work together (good control of interface dynamics)

## Slide 41
Need more robust photosensitizers (PS).
Thus POM-based MPCT and MMCT chromophores
Requirements for viable PS:
Absorbs sunlight intensely and broadly
Charge-separated excited state (exciton)
Long-lived charge-separated excited state
Metal-to-Polyoxometalate (MPCT)
Chromophores.
J. Am. Chem. Soc. 2011, 133, 20134–2013

## Slide 42
(a) X-ray structure of [P4W35O124{Re(CO)3}2]16– in combined polyhedral and ball-and-stick notation. Re: yellow; O: red; C: black; WO6 octahedra: gray; PO4 tetrahedra: purple. (b) UV–Vis and (c) FTIR spectra of in CH2Cl2.
The calculated HOMO and LUMO of the model complex [{P2W18O63[Re(CO)3]}(H2O)(OH)]8-.
J. Am. Chem. Soc. 2011, 133, 20134
New class of photosentizer (metal-to-POM CT)

## Slide 43
Average transient visible (a), and mid-IR (b, 0~5 ps; c, 5~100 ps) absorption spectra in CH2Cl2 at indicated delay time windows after 400 nm excitation.
Arrows in (b) and (c) indicate the directions of amplitude changes.
Time-resolved spectroscopic studies
reduced POM unit
EXCITATION:
New bands: 1925, 2020 cm-1: blue-shifted (electron density on Re is decreased)
DECAY:
New Bands: 1850, 1980 cm-1: red-shifted
(hot ground state; vibrational cooling process)

## Slide 44
Co2V2-POM: Light driven O2 evolution
Kinetics of O2 formation with 2 μM Co4V2 in light-driven reaction
1.0 mM [Ru(bpy)3]2+, 5.0 mM Na2S2O8, 80 mM borate buffers, pH 9
Expected (d[O2]/dt)/(d[Ru(bpy)3]3+/dt) = (Y/4) = 0.175 Determined 0.165
Experiment:
d[O2]/dt ~ 3.3x10-7 M/s
Y = 4[O2]/[Ru(bpy)33+]o ~ 0.7 for Co4V2
d[Ru(bpy)3]3+/dt ~ 2.0x10-6 M/s
Light driven O2 evolution rate is limited by oxidant generation

## Slide 45
dark
2): 1) + Co4P2-POM
1): a-Fe2O3
3): 2) + toluene wash
4): 3) + Co4P2-POM
1)
2)
3)
4)
Control: Films prepared with Co(NO3)2 or Co4P2-POM (without THpA) forms CoOx on electrodes. Photocurrent remains after toluene wash
Film preparation:
drop-cast Co4P2-POM:THpA toluene solution on α-Fe2O3 films
dry in air
wash with 1M NaOH
Hydrophobic immobilization and stabilization of POMs on semiconductor photoanodes (POM dyads)
(heptyl)4N+ immobilzes and stabilizes Ru4POM and Co4P2-POM on photoelectrodes (Fe2O3 and TiO2 )

## Slide 46
CT and water oxidation in POM-containing nanotriads
Semiconductor–PS-POM WOC Interfaces: Water-Oxidizing Photoelectrodes.
• Triad preparation
• Triad structure (including atomistic knowledge of the metal oxide surface)
• Photocurrent (H2O  O2)
• Charge transfer dynamics (experimental and computational)
John Fielden

## Slide 47
Evaluation of water oxidation catalytic activity
Light-Driven Water Oxidation by Sacrificial Electron Acceptor
2 S2O8 2- + 2 H2O + 2 hν → 4 SO4 2- + O2 + 4 H+
Water Oxidation (dark)
4 [Ru(bpy)3]3+ + 2 H2O → 4 [Ru(bpy)3]2+ + O2 + 4 H+
POM WOC
Photoelectrochemical cells: H2O + 4 hν → H2 + ½ O2

## Slide 48
Hill group POM WOCs (X-ray structures)
O
Ru
Co
Ni
Ir
Cl;
PO4/SiO4/GeO4
ZnO4/ZnO6
WO6
MoO6
Chem. Soc. Rev. 2012,
41, 7572–7589.

## Slide 49
Hill group POM WOCs (X-ray structures)
O
Ru
Co
Ni
Ir
Cl;
PO4/SiO4/GeO4
ZnO4/ZnO6
WO6
MoO6
Chem. Soc. Rev. 2012,
41, 7572–7589.

## Slide 50
[Co4(H2O)2(VW9O34)2]10- (Co4V2-POM)
Just published:
J. Am. Chem. Soc. 2014, 136, 9268
doi.org/10.1021/ja5045488
X-ray structure (R = 2.45%) Co, O, VO4, WO6
Lixin Wu

## Slide 51
Co2V2-POM: extremely fast WOC (TOF > 1000 sec-1)
Reduction of [Ru(bpy)3]3+ to [Ru(bpy)3]2+ followed at 670 nm with stopped-flow system. Conditions: 1.0 mM [Ru(bpy)3]3+, 1 µM catalyst, 40 mM borate buffer pH = 8.0.
4 [Ru(bpy)3]3+ + 2 H2O → 4 [Ru(bpy)3]2+ + O2 + 4 H+

## Slide 52
Catalytic Water Oxidation.
Potentiometric Titration of Co4P2 with Co(III)W12
1 mL of 2 mM Co(III)W12 was titrated by 2 mM Co4P2 in 80 mM sodium borate buffer pH 8.0.
Co(III)W12 + Co4P2(i) =
Co(II)W12 + Co4P2(i+1)
i = 0-2
Estimated potentials versus Ag/AgCl:
E1o(Co4P2(I))/(Co4P2(0)) = (1.1±0.02) V
E2o(Co4P2(II))/(Co4P2(I)) = (1.07±0.02) V
Eo(Co(III)W12)/(Co(II)W12) = 1.05 V (NHEl)

## Slide 53
Co4P2 not stable under electrocatalytic conditions
Scandola, Bonchio et al. Chem. Commun., 2012, 48, 8808:
50 mM Co4P2 rate of photogenerated [Ru(bpy)3]3+ reduction by Co4POM.
Stracke, Finke, J. Am. Chem. Soc., 2011, 133 , 14872:
500 mM Co4P2, electrocatalytic water oxidation at high bias.
4 experiments show Co4P2  CoOx
O2 not measured, TON not addressed.

## Slide 54
Catalytic Water Oxidation.
Potentiometric Titration of Co4P2 with [Ru(bpy)3]3+
50 μM Co4P2, 80 mM sodium borate buffer pH 8.0. The reaction was followed by formation of [Ru(bpy)3]2+ using a stopped flow instrument
Chart: 
| 0.5 | 1.0 | 2.0 | 4.0 | 6.0
 | 0.47273 | 1.0182 | 1.9455 | 2.8182 | 3.4545
 | 0 | 0.5 | 1 | 2 | 4 | 6
[Ru(bpy)3]3+ + Co4P2(i) = [Ru(bpy)3]2+ + Co4P2(i+1), i = 0-4
Estimated potentials versus NHE:
E3o(Co4P2(II))/(Co4P2(III)) = (1.25 ± 0.02) V
E4o(Co4P2(III))/(Co4P2(IV)) = (1.23 ± 0.02) V E3o > E4o

## Slide 55
Ongoing work
• polyoxometalate (POM) water oxidation catalysts (WOCs)
• POM WOC stability and reactivity
• photocatalytic POM-based dyads, triads
POM immobilization
• POM-based chromophores and photosensitizers (PS)
• POM H2O, CO2 reduction catalysts (noble-metal-free and
water compatible, molecular -- J. Am. Chem. Soc. 2014, 136, 14015)
• pH 14-compatible POM WOCs
• Counter cation effects on POM catalysis, immobilization
(molecular models for MOS electrode surfaces)

## Slide 56
Ongoing work
• polyoxometalate (POM) water oxidation catalysts (WOCs)
• POM WOC stability and reactivity
• photocatalytic POM-based dyads, triads
POM immobilization
• POM-based chromophores and photosensitizers (PS)
• POM H2O, CO2 reduction catalysts (noble-metal-free and
water compatible, molecular -- J. Am. Chem. Soc. 2014, 136, 14015)
• pH 14-compatible POM WOCs
• Counter cation effects on POM catalysis, immobilization
(molecular models for MOS electrode surfaces)

## Slide 57
POMs can address the many challenges for WOCs,
• fast and selective
4e
H2O
HO•
H2O2
O2•
O2
volts
electrons removed
1e
2e
3e
• stable
(air, water, heat)
• homogeneous
--interface with photosensitizer (PS) more controllable
--experimentally and computationally study molecular level; optimize
• inexpensive (earth-abundant metals)
• nontoxic and can mass produce
Notes: 57

## Slide 58
Confocal Raman Characterization of BiVO4-Ru4-POM
Conditions
Typical electrodes fabricated for PEC study
Electrode surface was rinsed with IPA and water
514 nm laser
~400 nm spot size
Ben Yin and Sarah Lauinger