## Slide 1
Ewa Bogel-Łukasik
Universidade Nova de Lisboa,
Foundation for Science and Technology (FCT), LAQV/REQUIMTE, Associated Laboratory for Green Chemistry, Portugal
ADVANCED FLUIDS in TAILOR-MADE BIOFUEL and BIO-BASED PRODUCT PROCESSING
Alternative Ionic Liquid-based Lignocellulosic Biomass
Pre-treatment and Fractionation towards Progress in Biorefinery
e-mail: ewa.lukasik@fct.unl.pt

## Slide 2: Where are we in an European Technology Platform supply chain (2015-2020 and beyond)?
2

## Slide 3
Why biomass is significant?
Supply energy for all kind of activities
Regulate essential activities of human systems
Fundamental chemicals in the plant kingdom

## Slide 4: Need of biomass raw materials
Many sectors want biomass raw materials
Transport/ biofuels compete with food and feed production regarding AGRICULTURAL CROPS
Best guaranted price
Best guaranted price
FREE!

## Slide 5: Biorefinery
www.processum.se
Today
Future

## Slide 6
United States Department of Energy Genome Programs/genomics.energy.gov
Cellulose
is like an iron frame to keep the structure of plants
Hemicellulose
is like a string to bind the cellulose fibers
Lignin
is like cement to harden the structure
Cellulose: 30-50% - crystalline homopolymer of glucose (cellobiose); difficult to chemically hydrolyse, susceptible to enzymatic attack by cellulases
Hemicellulose: 15-30% - heteropolymer made up of a variety of sugar units including glucose, xylose, galactose, arabinose and mannose; much easier depolymerised
Lignin: 10-25% - complex aromatic structure of cross-linked polymers of phenolic monomers; resistant to biochemical conversion; different depolymerisation chemistry
Lignocellulosic biomass
A complex biopolymer

## Slide 7: Formation of micro- and macrofibrils (fibres) of cellulose and their position in the wall
P.F.H. Harmsen, W.J.J. Huijen, L.M. Bermudez Lopez, R.R.C. Bakker, Literature review of Physical and Chemical Processes
for Lignocellulosic Biomass, ECN-E-10-013, 2010

## Slide 8
P.F.H. Harmsen, W.J.J. Huijen, L.M. Bermudez Lopez, R.R.C. Bakker, Literature review of Physical and Chemical Processes
for Lignocellulosic Biomass, ECN-E-10-013, 2010
Demonstration of the hydrogen bonding that allows the parallel arrangement of the cellulose polymer chains

## Slide 9
Pre-treatment of lignocellulosic biomass
Pre-treatments
Essential to disrupt the complex structure of lignocellulosic biomass
↑ Extraction of lignin
↓ Crystallinity of cellulose
↑ Surface area for enzyme binding and microbial attack
Types of pre-treatments:
Physical treatment (milling, gridding);
Chemical pre-treatments (alkali and acid hydrolysis);
Physico-chemical pre-treatments (steam explosion);
Biological pre-treatments.
Carvalheiro, F. et al., Appl. Biochem. Biotechnol., 2009, 153, 84-93; Yoon, L.W. et al., J. Chem. Technol. Biotechnol., 2011, 86, 1342-1348 http://genomicsgtl.energy.gov/biofuels/.

## Slide 10: Biorefinery and Green Chemistry complex role
Biomass
Increased Value
Biorefinery
Energy
Fuel Energy
Chemicals
Materials
Chemicals
SIADEB www.siadeb.org 2014
Green Chemi-stry
Prevention
Atom Economy
Inherently Safer Chemistry for Accident Prevention
Less Hazardous Chemical Syntheses
Designing Safer Chemicals
Safer Solvents and Auxiliaries
Design for Energy Efficiency
Use of Renewable Feedstocks
Reduce Derivatives
Catalysis
Real-Time Analysis for Pollution Prevention
Design for Degradation
P.T. Anastas and J.C. Warner, Green Chemistry: Theory and Practice, Oxford University Press, New York, 1998.

## Slide 11
Autohydrolysis
Dilute acid hydrolysis
Acetosolv/Organosolv
Alkaline
Ionic liquids
Common methods of biomass pretreatment

## Slide 12
Published Items in Each Year
ISI Web of Science report by THOMSON REUTERS
 | TOPIC: |  | 
 | 28/08/2015 |  | 
"ionic liquid*" |  |  | 101145
"ionic liquid*" and "biomass" |  |  | 1544

## Slide 13
Citations in Each Year
ISI Web of Science report by THOMSON REUTERS
The latest 20 years are displayed. | 
Results found: | 1544
Sum of the Times Cited: | 31564
Sum of Times Cited without self-citations: | 20891
Citing Articles: | 13344
Citing Articles without self-citations: | 12050
Average Citations per Item: | 20.44
h-index: | 80

## Slide 14
Pre-treatment of lignocellulosic biomass
Possible solution
ionic liquids
Why?

## Slide 15
Ionic liquids &biomass
Solubility
Efficient pre-treatment
Conversion of biomass carbohydrates into Value Added Products
Solubility & pre-treatment of biomass with ILs
Ability of an anion and a cation to interact with carbohydrates
Water content
Mutual interactions in raw biomass

## Slide 16
Ionic liquids
Anions
Cations
1018

## Slide 17
Properties of ILs can be tailored:
Density and Viscosity
Solubility
Lipophilicity and polarity
The toxicity and biodegradability of ionic liquids are an important issue
High polarity
Negligible volatility
Thermal stability
High conductivity
Large electrochemical window
Ionic liquid properties
Solvent power
Tunable solvation

## Slide 18
Role of Pre-treatment of raw feedstock with ILs
Benefits:
Alter the physicochemical properties of the biomass macromolecular components
Extract a specific macromolecular fraction
Perform different fractionation approaches after dissolution
↓ Cellulose crystallinity
↑ Extraction of lignin
Lower degradation of monosaccharides
Sustainable aspect due to the IL reuse and recycle possibility

## Slide 19
Pre-treatment of biomass with ILs
Rice straw
Triticale straw
Wheat straw
Sugarcane bagasse
Biomass
Ionic liquids
[emim]+
[bmim]+
[CH3COO]-
[SCN]-
[N(CN)2]-
[HSO4]-

## Slide 20
Pre-treatment of biomass with ILs
Rice straw
Triticale straw
Wheat straw
Sugarcane bagasse
Raw Biomass
Milled biomass
Wheat straw
Sugarcane bagasse
Rice straw
Triticale straw

## Slide 21: Methodology
21
Fractionation & recovery
120 oC, 6 h, 5 % (w/w)
Liquid Fraction
NaOH (0.1 M)
A method
Carbohydrates
Lignin
Cellulose
B method
Filtrate
Hemicellulose
Residual lignin
110 oC, 4 h, 2 % (w/w)
NaOH (3 %)
EtOH
HCl
HCl
Acetone/Water (9:1,( v/v))
Ionic liquid recovery
93 % (initial)
Wheat straw
[emim][CH3COO]
+
Ionic liquid recovery
73 % (initial)
A. M. da Costa Lopes, K. João, D. Rubik, E. Bogel-Lukasik, L. C. Duarte, J. Andreaus and R. Bogel-Lukasik, Bioresource Technol., 2013, 142, 198-208

## Slide 22: Methodology
A. M. da Costa Lopes, K. João, D. Rubik, E. Bogel-Lukasik, L. C. Duarte, J. Andreaus and R. Bogel-Lukasik, Bioresource Technol., 2013, 142, 198-208
Fractionation & recovery
Liquid Fraction
Carbohydrates
Lignin
Cellulose
Filtrate
Hemicellulose
Residual lignin
NaOH (3 %)
EtOH
HCl
HCl
120 oC, 6 h, 5 % (w/w)
C method
Residual hemicellulose
Ionic liquid recovery
86 % (initial)
EtOH
NaOH (0.1 M)
Wheat straw
[emim][CH3COO]
+

## Slide 23: FTIR spectra of carbohydrate samples
800
1000
1200
1400
1600
1800
Wavenumbers (cm-1)
A
1034
1060
1112
1161
C-O
asymmetric bending
C-OH skeletal vibration
C-O-C skeletal vibration
C-O stretching vibration
898
β-glycosidic
C-H deformation
Cellulose MN 300 (standard)
989
1042
arabinosyl side chain vibration
xylan C-O-C contribution
Hemicellulose-rich
Cellulose-rich
Wheat straw
Lignin aromatic vibration
1508
1734
Ester linkage vibration

## Slide 24: FTIR spectra of lignin samples
800
1000
1200
1400
1600
1800
Wavenumbers (cm-1)
A
1032
Aromatic C-H
plane deformation
1127
C-H plane deformation in syringyl units
1508
1458
1420
1596
C-O vibrations
1225
1263
Aromatic skeletal vibrations
840
C-H out-of-plane deformation

## Slide 25: Advantages of the C method
C method was chosen
Method | A | B | C
% Purity cellulose | ↓ | ↓ | ↑
% Purity hemicellulose | ↓ | ↓ | ↑
% Loss carbohydrates | ↑ | ↑ | ↓
% Loss lignin | ↓ | ↓ | ↑

## Slide 26: Results with various ILs
Cellulose
Hemicellulose
Lignin
[emim][CH3COO]
[bmim][N(CN)2]
[bmim][SCN]
[bmim][HSO4]
Chart: 
| Carbohydrates | Lignin | Others
 | 0.86 | 0.06 | 0.08
Chart: 
| Carbohydrates | Lignin | Others
 | 85 | 5 | 10
Chart: 
| Carbohydrates | Lignin | Others
 | 0 | 87 | 13
Chart: 
| Carbohydrates | Lignin | Others
 | 0 | 100 | 0
ILs
Carbohydrates
Lignin
Others
NQ
Not quantified
Chart: 
| Carbohydrates | Lignin | Others
 | 0.68 | 0.06 | 0.26
Chart: 
| Carbohydrates | Lignin | Others
 | 70 | 6 | 24
Chart: 
| Carbohydrates | Lignin | Others
 | 0 | 89 | 11
Chart: 
| Carbohydrates | Lignin | Others
 | 0.87 | 0.08 | 0.05
Chart: 
| Carbohydrates | Lignin | Others
 | 85 | 9 | 6
Chart: 
| Carbohydrates | Lignin | Others
 | 0.9 | 0.03 | 0.07
Chart: 
| Carbohydrates | Lignin | Others
 | 0 | 100 | 0
Chart: 
| Carbohydrates | Lignin | Others
 | 0 | 62 | 38
Chart: 
| Carbohydrates | Lignin | Others
 | 0.624 | 0.18 | 0.197
Wheat straw
A. M. da Costa Lopes, K. João, E. Bogel-Lukasik, L. B. Roseiro, R. Bogel-Lukasik, J. Agric. Food Chem., 2013, 61, 7874.

## Slide 27: Quantitative FTIR results for fractionation of sugarcane bagasse with [emim][CH3COO]
Chart: 
K. João, A. M. da Costa Lopes, E. Bogel- Łukasik L. C. Duarte and R. Bogel-Lukasik, 2015, in preparation.
Carbohydrates
Lignin
Others
SF, LF: solid or liquid fraction
ML: material lost
RM: regernerated fraction

## Slide 28: Results with other types of biomass
Chart: 
| Carbohydrates | Lignin | Others
 | 0.679 | 0.2052 | 0.1158
Chart: 
| Carbohydrates | Lignin | Others
 | 0.651 | 0.144 | 0.205
Chart: 
| Carbohydrates | Lignin | Others
 | 0.692 | 0.201 | 0.107
Chart: 
| Carbohydrates | Lignin | Others
 | 0.624 | 0.18 | 0.197
Cellulose
Hemicellulose
Lignin
Wheat straw
Rice straw
Sugarcane bagasse
Triticale straw
Chart: 
| Carbohydrates | Lignin | Others
 | 0.86 | 0.06 | 0.08
Chart: 
| Carbohydrates | Lignin | Others
 | 85 | 5 | 10
Chart: 
| Carbohydrates | Lignin | Others
 | 0 | 87 | 13
Chart: 
| Carbohydrates | Lignin | Others
 | 0.9 | 0.07 | 0.03
Chart: 
| Carbohydrates | Lignin | Others
 | 93 | 6 | 1
Chart: 
| Carbohydrates | Lignin | Others
 | 0 | 66 | 34
Chart: 
| Carbohydrates | Lignin | Others
 | 0.95 | 0.05 | 0
Chart: 
| Carbohydrates | Lignin | Others
 | 89 | 3 | 8
Chart: 
| Carbohydrates | Lignin | Others
 | 0 | 100 | 0
Chart: 
| Carbohydrates | Lignin | Others
 | 0.9 | 0.06 | 0.04
Chart: 
| Carbohydrates | Lignin | Others
 | 90 | 10 | 0
Chart: 
| Carbohydrates | Lignin | Others
 | 0 | 71 | 29
Biomass
Carbohydrates
Lignin
Others
NQ
Not quantified
K. João, A. M. da Costa Lopes, E. Bogel- Łukasik L. C. Duarte and R. Bogel-Lukasik, 2015, in preparation.

## Slide 29
Enzymatic Hydrolysis: A,B, C methods
Enzymes:
Celluclast® 1.5L
Novozym 188
Conditions:
50oC, 72h, 150rpm
WS – wheat straw; AH – acid hydrolysed; RM – regenerated material; STD - standard
%
A. M. da Costa Lopes, K. João, D. Rubik, E. Bogel-Lukasik, L. C. Duarte, J. Andreaus and R. Bogel-Lukasik, Bioresource Technol., 2013, 142, 198-208

## Slide 30
Hemicellulose Hydrolysis of the biomass pre-treated with [bmim][HSO4]
Electropherograms showing the profile for a) diluted pure [bmim][HSO4] (1/5) at 210 nm, b) sample of the filtrate 1 from process with [bmim][HSO4] at 210 nm; c) diluted pure [bmim][HSO4] (1/5) at 270 nm; d) furfural and HMF identified in the sample at 270 nm; and e) furfural and HMF standard solutions at wavelengths at 270 nm.

## Slide 31: Enzymatic Hydrolysis: Sugarcane bagasse
Enzymes:
Celluclast® 1.5L
Novozym 188
Conditions:
50oC, 72h, 150rpm
AH – acid hydrolysed; Cellulose CA – cellulose obtained from sugarcane bagasse pre-treatment; STD - standard
%
K. João, A. M. da Costa Lopes, E. Bogel- Łukasik L. C. Duarte, R. Bogel-Lukasik, 2015, in preparation.

## Slide 32: Enzymatic Hydrolysis: Rice straw
Enzymes:
Celluclast® 1.5L
Novozym 188
Conditions:
50oC, 72h, 150rpm
AH – acid hydrolysed; Cellulose CB – cellulose obtained from rice straw pre-treatment; STD - standard
%
K. João, A. M. da Costa Lopes, E. Bogel- Łukasik L. C. Duarte, R. Bogel-Lukasik, 2015, in preparation.

## Slide 33: Enzymatic Hydrolysis: Triticale straw
Enzymes:
Celluclast® 1.5L
Novozym 188
Conditions:
50oC, 72h, 150rpm
AH – acid hydrolysed; Cellulose CC – cellulose obtained from triticale straw pre-treatment; STD - standard
%
K. João, A. M. da Costa Lopes, E. Bogel- Łukasik L. C. Duarte, R. Bogel-Lukasik, 2015, in preparation.

## Slide 34: Crystallinity indexes
Sample | LOI | TCI
WS | 1.74 | 1.13
SB | 1.57 | 1.18
RS | 1.76 | 1.15
TS | 1.74 | 1.14
WS AH | 1.68 | 1.07
SB AH | 1.58 | 1.05
RS AH | 1.60 | 1.10
TS AH | 1.81 | 1.01
RM WS | 1.36 | 1.02
RM SB | 1.27 | 1.04
RM RS | 1.45 | 1.10
RM TS | 1.55 | 1.08
Sample | LOI | TCI
STD cellulose | 1.69 | 1.12
Cellulose WS | 1.34 | 1.02
Cellulose SB | 1.31 | 1.07
Cellulose RS | 1.46 | 1.11
Cellulose TS | 1.59 | 1.10
+
-
Lignin/hemicellulose content also affects cellulose accessibility in enzymatic hydrolysis
WS – wheat straw; SB – sugarcane bagasse; RS – rice straw; T – triticale straw; AH – acid hydrolysed; RM– regenerated material; STD - standard ; LOI – lateral order index ; TCI – total crystallinity index 34
+
-
LOI
TCI
Nelson, M.L. et al., J. Appl. Polym. Sci. , 2003, 8 (3), 1325–1341
Hurtubise, F.G. et al., Anal. Chem.,1960, 32 (2), 177–1810

## Slide 35: [emim][CH3COO]IL recyclability in an efficient Pre-treatment of Wheat Straw
good recyclability of ILs
A. M. da Costa Lopes, K. João, D. Rubik, E. Bogel-Lukasik, L. C. Duarte, J. Andreaus and R. Bogel-Lukasik, Bioresource Technol., 2013, 142, 198-208

## Slide 36: Are other ILs recovery in pre-treatment of Wheat straw is also sufficient?
A. M. da Costa Lopes, K. João, E. Bogel-Lukasik, L. B. Roseiro and R. Bogel-Lukasik, J. Agric. Food Chem., 2013, 61, 7874.
a WS, wheat straw; b SF, solid fraction; c LF, liquid fraction; d RY, regeneration yield; e residual.

## Slide 37: Conclusions
A 3-step optimised fractionation using [emim][CH3COO] for 4 types of biomass was tuned to obtain separately cellulose, hemicellulose and lignin as high purity samples
[bmim][HSO4] posses a capability to dissolve wheat straw completely
and hydrolyse hemicellulose selectively to produce furfural and hydroxymethylfurfural confirming extended hydrolyses of sugars
Pre-treatment of wheat straw using [bmim][SCN] gives lignin-rich materials with a high purity of lignin (no carbohydrates)
Importance to fractionate the liquid stream after the regeneration process within pre-treatment of biomass with IL to recover remaining significant amount of hemicellulose and lignin
Combined method allowed to produce carbohydrate-rich material and a carbohydrate-free lignin more efficiently and can suit as a direction in development of an industrially feasible pre-treatment and fractionation of biomass

## Slide 38: Conclusions
Reduction in cellulose crystallinity (LOI) implies that treated with the IL cellulose material has a cellulose surface accessibility increased that what confirmed by efficiency of hydrolysis
IL recyclability 7 times without losses in biomass pre-treatment efficiency for WS (up to 95% for [emim][CH3COO] ) , for other biomass up to 97% ([bmim][N(CN)2] ).
LOI decrease of biomass pre-treated with ILs might indicate restruction of crystalline structure of cellulose rich materials into amorphous forms
Easy digestible material was regenerated from all 4 types of biomass pre-treated with the IL.
The partial delignification of biomass enables to achieve complete hydrolysis into reducing sugars. IL pre-treatment is more efficient than the conventional acid hydrolysis pre-treatment.

## Slide 39: Acknowledgments
Fundação para a Ciência e a Tecnologia, Portugal
IF/01643/2013/CP1161/CT004
SFRH/BPD/26356/2006
PEst-C/EQB/LA0006/2011
Programme Ciência 2008
UID/QUI/50006/2013
SFRH/BD/90282/2012
IF/01643/2013
LAQV/REQUIMTE
National NMR Facility (RECI/BBBBQB/0230/2012)

## Slide 40: Acknowledgments
FPS COST Action FP1306: Valorisation of lignocellulosic biomass side streams for
sustainable production of chemicals, materials & fuels using low environmental impact technologies
COST Actions: CM 1304 Emergence and Evolution of Complex Chemical Systems
LNEG
ERA-IB project Products from lignocelluloses
PROETHANOL2G Project (FP7-ENERGY-2009-BRAZIL;Grant agreement: 251151)
Brazilian National Council of Scientific and Technological Development

## Slide 41: Acknowledgments
André da Costa Lopes
Karen G. João
Ewa Bogel-Łukasik
Luísa B. Roseiro
Rafał Bogel-Łukasik
Luis C. Duarte
Djonatam Rubik
Jürgen Andreaus
Florbela Carvalheiro
Maria do Céu Penedo
Luísa Ferreira
Thank you!