## Slide 1
Comparing the Effect of Ecofriendly Adsorbents and Bioturbators on the Concentration of Pyrene
Febee Louka
Department of Chemistry
University of Louisiana at Lafaytte

## Slide 2
Gulf of Mexico
BP oil spill
Atlantic Empress
Oil Spills:
http://nypost.com/2014/10/27/bp-oil-spill-left-big-bathtub-ring-on-sea-floor/

## Slide 3
Effect of oil spills:

## Slide 4
Oil spill treatment:
The most common treatment of oil spills is using dispersants such as Corexit
Corexit 9500 was found to be lethal for silver fish which is used as a bench mark in toxicity testing.
The skin becomes red, swollen, and sore, sometimes with small blisters.
Dermatitis
Super bug causing MRSA like infection
http://www.floridaoilspilllaw.com/toxicologist-oil-eating-microbes-genetically-modified-mrsa-like-infection/

## Slide 5
Corexit oil residue promotes the absorption of toxins into the skin. The contamination into the skin are not visible under normal light, but show appear as fluorescent spots under UV light
Another type of unknown rash appears in the form of bumps. Then a raw, irritating redness sets in before the skin peels away in patches. Accompanied with other symptoms, such as dizziness, nausea, diarrhea and bloody stools
http://news.discovery.com/earth/corexit-bp-120419.htm

## Slide 6
The most used energy in the world
Causes many problems like global warming and oil spill
Oil spills cause some damages and pollution
16 of them are considered as priority pollutants by USEPA
They form DNA adducts in living organisms which can induce mutations
Deadly for marine animals and human due to bioaccumulation
Oil Spills and Polycyclic Aromatic Hydrocarbons (PAHs)
Oils
PAHs

## Slide 7
Bioturbators
Biological Treatment

## Slide 8
What are Bioturbators?
The ghost shrimp Lepidophthalmus louisianensis is one of the most-abundant bioturbators on the Gulf Coast, they move up to 3500 g sediment/m2/day and they make burrows up to 3 m deep.
The other bioturbator is the bivalve Tagelus plebeius (razor clam) which is present along the Gulf Coast. These clams also have the potential to affect contaminant distribution and biodegradation

## Slide 9
Determination of Pyrene in Presence of Bioturbators:
In this the study, research was conducted in laboratory greenhouse mesocosms containing field-collected clean water and sediment.
To determine the optimum duration and conditions for performing the experiment, An experiment was conducted over a time span of 33 days, in the presence and absence of ghost shrimp.

## Slide 10
Samples Analysis:
Water Samples Analyses
Liquid-liquid extraction (LLE) using (CH2Cl2).
After evaporation, the residue was dissolved in hexane.
Excess hexane was evaporated under N2 to 1.00 mL.
Sediment Samples Analyses
Dry Sediment + CH2Cl2

## Slide 11
Microwave extraction using the US EPA 3546 method.
Filtration
Rinsing
Evaporation
The residue was dissolved in hexane
Excess hexane evaporated under N2 to 1.00 mL.
An Aliquot injected
GC

## Slide 12
Biological Treatment
Results & Discussion

## Slide 13
Determination of Pyrene in Presence of Bioturbators
Water Samples In Abscence of Shrimp
Decrease in pyrene concentration from 12.07 to 3.15 μg/L after 10 days
Evaporation of pyrene due to high temperature

## Slide 14
Determination of Pyrene in Presence of Bioturbators
Water Samples In Presence of Shrimp
Shrimp
After 1 day concentration dropped to 2.72 μg/L
Ghost Shrimp that move up 3500 g sediment/m2/day
Evaporation of pyrene due to high temperature
After 10 days concentration determined was 2.68 μg/L
The pyrene evaporating is replaced by pyrene transported by shrimp to sediment

## Slide 15
Water Samples In Abscence of Razor Clams
Decrease in pyrene concentration from 17.88 to 11.25 μg/L after 10 days
Evaporation of pyrene due to high temperature
Pyrene (μg/L)
Water Day 10

## Slide 16
Water Samples In Presence of Razor Clams
Decrease in pyrene concentration from 12.8 to 5.7 μg/L after 10 days
Presence of clams
Evaporation of pyrene due to high temperature
Pyrene (μg/L)

## Slide 17
Sediment Samples In Abscence of Shrimp
For surface sediment, there difference in pyrene concentration is not significate different between day 1 and day 10
Evaporation due to high temperature
Very low transportation of Pyrene from surface sediment to subsurface sediment by the action of water movement
As for subsurface sediment the pyrene concentration parley increased between day 1 and day 10

## Slide 18
Sediment Samples In presence of Shrimp
Significant difference between day 1 and day 10 for surface sediment
Ingestion by the ghost shrimps
Adsorption on the surface of the shrimp
Degradation of pyrene by the shrimp
Pyrene transportation from surface sediment to subsurface sediment by the action of shrimp
Increasing of pyrene concentration in subsurface between day 1 and day 10

## Slide 19
Ecofriendly Treatment

## Slide 20
Effect of Exposure to Sugarcane Bagasse and Crawfish Shells:
The water samples were dosed with a known concentration of pyrene, and were treated with sugarcane “Saccharum officinarum” bagasse and crawfish “Cambarus robustus“ shells to examine their effects as adsorbents to remove oil pollutants from water samples.

## Slide 21
Effect of Time of Exposure on Pyrene Concentration:
Half a gram of sugarcane bagasse or one gram of crawfish shells were added to different containers with 400 mL of dosed pyrene solution.
Samples were shacked (250 R/M)
In case of crawfish shells, the concentration of pyrene was determined certain periods of time (12 hour, 1 day, 4 days, and 7 days)
In case of sugarcane bagasse, the concentration of pyrene was determined after different intervals of time (0.5 hour, 1 hour, 2 hours, and 24 hours)

## Slide 22
Ecofriendly Treatment
Results & Discussion

## Slide 23
Time of Exposure to Sugarcane Bagasse
Minutes

## Slide 24
Pyrene concentration decreased a lot in presence of sugarcane bagasse, due to it’s adsorption on the surface of the bagasse particles
By day 1: the concentration of pyrene droped to 16.8 μg/L compared to 434.3 μg/L at the beginning of the experiment (26 times less)
Effect of Time of Exposure to Sugarcane Bagasse

## Slide 25
Time of Exposure to Crawfish Shells
Minutes

## Slide 26
Effect of Time of Exposure to Crawfish Shells
Pyrene concentration decreased in presence of Crawfish Shells, due to it’s adsorption on the shells particles
On day 7, crawfish shells particles started to release part of the adsorbed pyrene

## Slide 27
Effect of Mass of Adsorbant on Pyrene Concentration:
Different masses of sugarcane bagasse or crawfish shells were added to different containers with 400 mL of dosed pyrene solution.
Samples were incubated
with sugarcane bagasse
for 1 day and for 2 days
in case of crawfish shells
at room temperature.
Mass of sugarcane bagasse (g)
μg pyrene/L
adsorbed by this amount.
When 0.5 g of sugar-cane bagasse was used almost all pyrene was

## Slide 28
μg pyrene/L
Mass of crawfish shells (g)
Effect of Mass of Crawfish Shells on Pyrene Concentration
Effect of Different Masses of Crawfish Shells
It took two days and 4 g of crawfish shells to almost remove (adsorb) all the pyrene from the water sample, leaving only traces

## Slide 29
Conclusions:
Biological and ecofriendly adsorbents are much safer than dispersants as a solution for oil spills.
Ecofriendly adsorbents are very promising method to remove PAHs.
Sugarcane bagasse is more efficient than crawfish shells, and both of them are very safe for the environment, animals and human.
Crawfish shells will start releasing the adsorbed pyrene after the 4th day of incubation.
The efficiency of the ecofriendly adsorbents should be tried with other PAHs.

## Slide 30
The grant from BP/The Gulf of Mexico Research Initiative
Dr. Paul Klerks
The Department of Chemistry at ULL
The Department of Biology at ULL
All my students
Acknowledgements

## Slide 31
Jullian
Chase
Paul
Ashley
Mark
Jeanne
Yasser
Jill
Marie
Guénaëlle
Gerard
Raven

## Slide 32
Kru
Dominique
Jodie
April
Mohamed
Alpha
Jorden
Eric
Ashley
Raven
Fatima
Amalia

## Slide 33
Thank you for your Attention
Questions