## Slide 1
OMICS 2015: Green Chemistry
Improvements to the Biorefinery Model Through Lignin Valorization
Ian Klein, Ph.D
Spero Energy, Inc.

## Slide 2: Spero Energy, Inc.
Initiated Operations in 2013
Advantage Sourced Raw Materials
Sustainable Catalysis
High Value Chemical Production

## Slide 3: Team Spero & Advisory Board
Barron Hewetson
Engineer
Ian Klein, Ph.D
Senior Scientist
Trenton Parsell, Ph.D.
Senior Scientist
Mahdi Abu-Omar, Ph.D.
Founder and President
Nathan Mosier, Ph.D.
Scale-up, bioprocess engineering
Robert Bedoukian, Ph.D.
President, Bedoukian Research Inc.
Research Institute for Fragrance Materials
Product validation & Development
William Ludlum
Managing Director, Hexagon Agency LLC
Commercial relationships & Product Development
Fabio Ribeiro, Ph.D.
Professor of Chemical Engineering, Purdue University
Process Development & Reaction Engineering
Eyal Barash, JD
Barash Law
Legal Counsel

## Slide 4
Lignin
Biomass2energy.com
Carbohydrates
Petrixo.com
$40 per ton
$40,000 per ton
Wasted Carbon Value
Notes: The plant component lignin is underutilized
Lignin must be removed in biorefiniery and paper pulp industries
Millions of tons of lignin are burned annually for low value energy
Low carbon efficiency of operations

## Slide 5
Linkage Types
β-O-4
5-5
α-O-4
β-5
8-8
Complex Structure & Low Selectivity

## Slide 6: SPERLUTM Technology
SPERLUTM
Liquid stream
xylose
soluble lignin
Solid Phase
cellulose
unknown
Selective Process for Efficient Removal of Lignin and Upgrading

## Slide 7
Alcohol solvent
35 bar H2, 225o C,
Catalyst
Milled wood
Biomass Type | % Lignin Content |  |  | % Yield
Poplar WT-LORRE | 19.2 | 45 | 55 | 54
WT-Lodgepole Pine | 30.5 | 100 | NA | 19
WT-White Birch | 15.8 | 31 | 69 | 52
Eucalyptus | 23.6 | 30 | 70 | 56
Selectivity
DHE
DMPP
SPERLUTM Yields
Biomass Type | % Lignin Content |  |  | % Yield
Poplar WT-717 | 18.5 | 31 | 69 | 40
Poplar 717-0998 (High G Poplar) | 18.7 | 90 | 10 | 27
Poplar 717-F5H (High S Poplar) | 20.2 | 17 | 83 | 37

## Slide 8
Chart: Glucan Yield vs Hydrolysis Time
| 0 | 1 | 6 | 18 | 72
Poplar residue | 0 | 37.611 | 55.9769 | 86.0538 | 80.27
Eucalyptus Residue | 0 | 15.4547 | 46.3428 | 76.492 | 77.5714
Poplar | 0 | 8.1522 | 9.4326 | 14.6392 | 11.2136
Eucalyptus | 0 | -1.6105 | -0.41656 | 2.1278 | 4.7946
Conditions:
200 mg glucan
citrate buffer, pH 4.8
CTEC-3 cellulase (50fpu)
50oC, 72 hours
Cellulose is not destroyed during HDO process
Cellulose residue amenable to hydrolysis
  Lignin inhibits enzymatic hydrolysis
Hydrolysis of SPERLUTM Residue

## Slide 9: SPERLUTM Advantages
Natural and renewable feedstock
Earth-abundant and recyclable catalyst
Easily separable product stream of aroma chemicals
Digestible carbohydrate co-product
Cost competitive

## Slide 10
Biorefinery Vision
T. Parsell, et al. Green Chem., 2015, 17, 1492-1499

## Slide 11
Business Opportunity
Chart: 
 | 375 | 300 | 440
DMP $375 M
Vanillin $300 M
Eugenol Family
$443M
$1.1 Billion Market
Flavor & Fragrance
Fragrance $10 B
  4.3% growth
Flavor $10.6 B
  6% growth
  Natural flavors 12%
Notes: High Value Renewable Specialty Chemical Production
  HVCs from wood waste
HVCs used in flavor & fragrance industry
  Spero HVCs and derivatives
    $400 M
Spero has inherently lower cost base

## Slide 12: Production Cost vs Product Value: DHE/DMPP
Total Product Value = $2180
1000 Kg Biomass
100 Kg DHE/DMPP
$2000
400 Kg Cellulose
$80
200 Kg Xylose
$100
Materials &
Process: $519

## Slide 13: Summary
High value products from Lignin
Enhanced digestibility of cellulose
Abundant, recyclable catalyst
Dedicated and Qualified Team
  Scientific and business acumen

## Slide 14: Acknowledgements
SBIR Phase II DOE (04/2015)
SBIR Phase I DOE (02/2014)
  Indiana matching grant (10/2014)
SBIR Phase I NSF (07/2014)
  Indiana matching grant (10/2014)
Phase IB NSF (12/2014)
BDM Business Plan Competition (02/2015)
Indiana BioCrossroads Prize (11/2014)
Clean Energy Trust : Midwest Clean Energy Challenge
  Indiana Clean Energy Challenge Winner (02/2014)
  Aviation Energy Prize Winner (05/2014)
Questions?
Notes: INVESTMENT