## Slide 1
Novel lignocellulosic hydrolyzate detoxification process using pyrochar from digestate: Application for bioethanol fermentation
F. Monlau, C. Sambusiti, A. Barakat
Past and Present Research Systems of Green Chemistry
September 14-16/2015 Orlando (USA)

## Slide 2
What is Anaerobic digestion ?
AD process characteristics
Temperature: ≈35°C (mesophilic), ≈ 50°C (thermopilic)
pH ≈ 6,5-7,5
HRT ≈ 60-100 days-1
Biogas
Digestate
An anaerobic biological process using anaerobic micro-organisms to convert biomass into biogas and digestate
● mainly composed of CH4 (55–75%) and CO2 (25–45%)
● Farm scale: CHP conversion with around 35% electricity efficiency.
● mixture of microbial biomass and undigested material.
● around 45% to 75% of the initial organic matter feed.

## Slide 3
Anaerobic digestates valorization
F. Monlau. New opportunities for agricultural digestate valorization: review and perspectives. Energy&Environmental Science (2015).

## Slide 4
Dual AD/Pyrolysis concept

## Slide 5
Dual AD/Pyrolysis concept
?
Energetic and mass balances of the dual AD/pyrolysis process
for one day- running

## Slide 6
Use of pyrochar as bio-adsorbents
SBET | Vmi | Vtot | Vmi/Vtot
(m2/g) | (cm3/g) | (cm3/g) | (%)
88 | 0.039 | 0.055 | 71

## Slide 7
Synthetic Medium: 10 g L-1 glucose; 1g L-1 furfural; 1g L-1 5-HMF; 24h
Lignocellulosic hydrolyzate detoxification
Chart: Removal (%)
| 5 g/L | 10 g/L | 20 g/L | 40 g/L | 60 g/L
5-HMF | 31.9216 | 39.2991 | 61.0785 | 97.5785 | 99.0434
Furfural | 34.9712 | 52.7687 | 86.6414 | 99.4372 | 100
Pyrochar concentration (24h)
Time adsorption (40g/L)

## Slide 8
Detoxification of corn stalk hydrolyzate
Corn stalks hydrolyzate:
150°C, 30 min, 5% (w/v) H2SO4
Pyrochar concentration : 60g L-1
Compounds | Corn stalks hydrolyzate
Glucose (g L-1) | 3.53 (±0.02)
Xylose (g L-1) | 5.23 (±0.05)
∑soluble sugars (g L-1) | 8,76
Acetate (g L-1) | 2.02 (±0.06)
Formic Acid (g L-1) | 0.15 (±0.04)
5-HMF (g L-1) | 0.12 (±0.00)
Furfural (g L-1) | 2.92 (±0.01)
∑Furans (g L-1) | 2,94
Chart: Removal efficiency (%)
| Pyrochar 1 | Pyrochar 2
Acetic acid | 14 | 14
Formic acid | 73 | 87
5-HMF | 100 | 100
Furfural | 91 | 93

## Slide 9
Simultaneous detoxification
and fermentation
Chart: Tme (h)
| 0 | 1 | 3 | 7 | 24
Eth-S2 | 0 | 1.3627 | 2.171 | 3.1645 | 4.2122
Eth-S2-Pyrochar | 0 | 1.3557 | 2.6563 | 4.2521 | 4.2771
Fur-S2 | 2.5 | 2.3158 | 1.7412 | 1.3234 | 0.19549
Fur-S2-Pyrochar | 2.5 | 0.61203 | 0.17158 | 0 | 0
Chart: Tme (h)
| 0 | 3 | 5.5 | 7.5 | 24
Eth-S1 | 0 | 1.5829 | 3.8212 | 4.4314 | 4.3572
Fur-S1 | 2.5 | 2.0104 | 0.12244 | 0.02885 | 0.02885
Eth-S1-Pyrochar | 0 | 4.2506 | 4.3663 | 4.2729 | 4.2334
Fur-S1-Pyrochar | 2.5 | 0.12085 | 0 | 0 | 0
Synthetic Medium: 8g L-1 glucose; 2 g L-1 xylose; 2,5 g L-1 furfural; 0,5 g L-1 5-HMF; 1 g L-1 acetate
Pyrochar: 60g L-1
Eth Strains: 30g L-1
S. Cerevisae “Red Ethanol”
S. Cerevisae “Lalvin ICV-K1”

## Slide 10
CONCLUSIONS
PERSPECTIVES
● Study the inpact of mechanical activation (i.e ball milling, vibro ball milling) on digestate pyrochar characteristics.
● Test the simultaneous detoxification and fermentation process at lower ethanol strains concentration.
● The dual AD/pyrolysis led to an electricity increase of 42% compared to AD alone.
● The simultaneous and fermentation process was efficient in improving the ethanol production rate.
● Extent the used of such pyrochars to the adsorption of phenolic compounds (i.e vanilin, syringaldehyde).
● Pyrochar from digestate were selective towards furans compounds. Furfural compounds were adsorbed at a faster rate than 5-HMF compounds.

## Slide 11
Thanks for your attention !
Monlau Florian
(monlau@supagro.inra.fr)
Past and Present Research Systems of Green Chemistry
September 14-16/2015 Orlando (USA)