## Slide 1
Photo redox catalysis
Catalytic pyrolysis and hydropyrolysis
Enzymatic hydrolysis
Thermochemical conversion of biomass
Biochemical conversion process
Lignocellulosic biomass gasification
Pyrolysis of alkali pre-treated biomass
Reaction engineering kinetics and catalysis
Block copolymer self-assembly
Free radical photopolymers
Rapid Catalyst screening using a high pressure, tandem µ-Reactor
R.R. Freeman(1), Chu Watanabe(1), Young-Min Kim(1), Prof. Norio Teramae(2)

## Slide 2
New catalysis are key to the long term conversion to sustainable, “green” products
Green products
Sustainability
Catalysts
 Dependable long term access to biomass
 Competitive economics
 Creation of new products
 “market acceptance”
Equivalent performance to petroleum based products
 Stable “bio” chemistry
 Stable geopolitics

## Slide 3
Why convert to “bio” feedstock?
Convert ‘waste” to products
Eliminate hazardous by-products from the environment
Eliminate by-products affecting human health
“Almost everything in your daily life depends on catalysts.” – Argonne National Laboratory
What do catalysis do?
Lower amount of energy needed for a chemical reaction
Lower production costs
Worker safety

## Slide 4
● Contnuous search for new catalysts – one that works “better” than those being used for a given process
● Test parameters
Temperature
Surface area (contact time)
Atmosphere
Pressure
Effective life time
Activity regeneration
● Rapid screening of new catalysts is essential if sustainable “green” products are going to exist in the future.
Catalyst characterization

## Slide 5
The typical catalyst evaluation system is designed around a large “furnace”. Changes in temperature may require 3 - 5 hr. before the system is stable enough to perform the needed test. A comprehensive catalyst evaluation normally requires a week or more.
http://www.j-science.jp/
2 m
Catalyst characterization: The old and the new
Tandem µ-Reactor
with Shimadzu QP2010 Plus GC-MS

## Slide 6
Single µ-Reactor
GC Oven
Furnace
Interface
Catalyst
Catalyst reaction
tube (quartz)
Split vent
Selective sampler
MicroJet cryo-trap
Separation column
MS
Reaction Gas
User selected parameters
µ-Reactor: - Catalyst
- type of atmosphere
- temperature
- pressure
- particle size
Reactor GC interface:
- type of carrier gas
- temperature
- split ratio
Notes: Are you certain there is a SS tube in 1st reactor?

## Slide 7
(40mm)
µ-Reactor: 100ºC ( 2nd- ITF: 250ºC)
µ-Reactor: 200 & 300ºC ( 2nd- ITF: 300ºC)
µ-Reactor: 400-900ºC (2nd- ITF: 350ºC)
120mm
Carrier or Reaction gas
ITF heater
µ-Reactor
GC INJ.
Catalytic bed temperature profiles [100 - 900⁰C]
Catalytic bed temperature at various points
0
20
40
60
80
100
120 mm
100
300
500
700
900ºC
100
200
300
400
500
600
700
800
900
1000ºC
Catalytic bed
temperature
GC DET.

## Slide 8
Temperature control/deviation and furnace heating/cooling
ZSM-5
(20/30 mesh)
ΔT : Max temp. deviation of A_B_C：<3ºC
Temperature control: ±0.1ºC
Thermocouple
78
50
60
A
B
C
70
He 50 ml/min
0.5ºC
100℃
200℃
400℃
Precisely controlled temperatures
ºC
100
200
300
400
10
20
30
ΔT: 0.0ºC
ΔT: 1.5ºC
ΔT: 2.9ºC
ΔT: 3.0ºC
40
900ºC
50
500
0
10
20
30 min
50 - 900ºC then cool to 50ºC
50 - 500ºC then cool to 50ºC
500 to 100ºC
<10 min
100
50 min

## Slide 9
3 Reactor heating profiles
Temperature control and two analytical modes of Tandem µ-Reactor
On-line EGA-MS analysis
time
Temp
Isothermal
EGA-Selective zone GC/MS analysis
Oven: Isothermal (300ºC)
EGA tube
(L=2.5 m, 0.15 Φ)
He
Aux
Vent-free
adaptor
GC column
(L=30 m, 0.25mm)
He
Aux
Selective
sampler
Reactor temp progr.
Oven: temp program.
Multi-linear
Stepwise
Notes: Residence time is the average amount of time a particle spends in a particular system.
In this case, the system means the reactor.

## Slide 10
Separation analysis
“ Stepwise temp. mode ”
Online – MS analysis
“ Linear temp. mode ”
TIC
1st µ-Reactor: 100ºC,
2nd µ-Reactor: 100-400ºC (20 ºC/min)
Catalyst: H-ZSM-5
Ethylene
(m/z 28)
Diethylether (m/z 74)
Ethanol (m/z 45)
Water
(m/z 18)
100
200
300
400ºC
2nd µ-Reactor temp.
Peak Area
2nd µ-Reactor temp.
Ethylene
Ethanol
Diethyl ether
300
400ºC
100
200
H2O
Reaction temp. vs. Peak area
1.0
2.0
3.0
4.0 min
300
100
200
400ºC
Ethylene
H2O
Ethanol
Diethyl ether
Time
1st µ-Reactor: 100ºC,
2nd µ-Reactor: 100, 200, 300, 400ºC (1sec)
Catalytic conversion of ethanol to ethylene

## Slide 11
GC Oven
2nd Reactor
2nd Interface
Catalyst
Catalyst reaction
tube (quartz)
Split vent gas OUT
Selective sampler
MicroJet Cryo-Trap
Separation column
MS
Carrier gas or
reaction gas
1st Reactor
1st Interface
Stainless steel tube
(deactivated with quartz)
Sample introduced
Tandem µ-Reactor
User selected parameters
1st reactor: SMPLE PREP
- type of atmosphere
- temperature
- pressure
-particle size
Reactor interface:
- Temperature
- type of atmosphere
2nd reactor:
- temperature
- Catalyst
- residence time??
Reactor GC interface:
- type of carrier gas
- temperature
- split ratio
Reaction Gas
Notes: Are you certain there is a SS tube in 1st reactor?

## Slide 12
Column: DX30-15M-0.15F, He: 1 ml/min, 1/50, GC: 70(0)-@15-320ºC(10 min), PY: 550ºC (ITF: 320ºC)
Transformation of Jatropha “press cake” to “BTEX”
Jatropha sample and Zeolite catalyst was provided by Dr. Murata of energy group of AIST, Japan
1.8x106
1.0
2.0
3.0
4.0
5.0
6.0
7.0
8.0
9.0
10.0
11.0
12.0
Pyrogram of Jatropha (0.55 mg) at 550℃
Hexadecadienoic acid
Octadecadienoic acid
o-Methoxyphenol
1,2-Cyclopentanedione
GC/MS
550ºC
（Flash Py）
He: 50 mL/min
Configuration
GC/MS
550ºC
（Flash Py）
550ºC
（Transformation）
He: 50 mL/min
Zeolite
Catalyst
5x106
0.5
1.0
1.5 min
Benzene
Toluene
Xylene
Ethyl benzene
Jatropha (0.55 mg) pyrolyzates from 1st Reactor flow into 2nd Reactor and transformed by catalyst
Bio-based fine chemicals

## Slide 13
Col.: Ultra ALLOY-5, 30 m 0.25 mm 1 um, GC Oven: 40 (2 min)- 40 ºC/min - 300ºC (2 min)
Cellulose (0.1 mg)
< Molybdenum – H2S activated >
C4
H2O
C2
C3
C5
C6
Cyclopentane
Me-cyclopentane
Bz
2.00
4.00
6.00
8.00
10.00
12.00
14.00
15.00 min
Tol
Xy
Naph.
p-Me-lbiphenyl
GC/MS
450ºC
（Flash Py）
200ºC
（Transformation）
Cryo-trap
He: 20 mL/min
Vent: 69 mL/min
H2: 50 mL/min
Sample cup
Conversion of “Cellulose” into bio-fuels by MoS2/Al2O3 catalyst – in hydrogen
Notes: 13

## Slide 14
GC
Cooling gas
Carrier
gas
Aux Gas
MFC
MS
LN2 trap
Split vent
EGA or
GC column
MFC
1st Reactor
2nd Reactor
Innovative pneumatics for HP Tandem µ-Reactor
OPTION
HP flow module
Sample
Sample cup/ALS (Solid)
Micro syringe (Gas/Liquid)
Micro feeder (Liquid)
Open split interface
Restrictor tube (deactivated)
(0.05 mm i.d., 1 m)
Vent
Vent
BP-1
Max
3.5 MPa
Vent
BP-2
Max
0.4 MPa
HP flow controller

## Slide 15
1
2
3
4
5
6 min
100
200
x100
a)
b)
c)
d)
e)
f)
g)
h)
1
2
3
4
5
6
7
8
9 min
100
200
300
400
Standard flow configuration (Direct connection)
0.10 MPa
Column:1.4 mL/min
Split ratio: 1/70
Column = 1.10 mL/min
Split ratio: 1/40
BP1: 0.5 MPa
BP2: 0.07 MPa
High pressure flow configuration (With restrictor and open split interface)
x20
b)
c)
d)
e)
f)
g)
h)
a)
1
2
3
4
5
6 min
x100
a)
200
400
600
800
0.4 MPa
b)
c)
d)
g)
h)
Column:11.6 mL/min
Split ratio: 1/10
i)
1
2
3
4
5
6
7
8
9 min
100
200
300
400
BP1: 3.0 MPa
BP2: 0.07 MPa
x10
i)
Column = 1.14 mL/min
Split ratio: 1/40
Column flow as a function of Reactor pressure
Notes: This slide shows the results of catalytic conversion of ethanol to ethylene using both the conventional and new methods at high pressures.
An FID detector was used for both conventional and new methods for comparison because MS cannot be used in the conventional method when the inlet pressure is 0.6MPa with column flow rate of over 10 ml/min.
In the conventional method, as the reactor pressure increases, the column flow increases.
Therefore, the retention times for the main component of ethylene and other products greatly changes and the resolution changes as the pressure increases.
On the other hand, in the new method, even when the reactor pressure changes, the retention times as well as column flow rate stay almost constant.

## Slide 16
Rotating
knob
Drop to 1st Reactor
Spring 1
Sample
Spring 2
Sample cup
Cup chuck
Standard solid sampler
Drop to 1st Reactor
Push button
High pressure solid sampler
80 µl cup
Sample is placed directly into the sample cup (Eco-Cup)
High pressure sample injection of solids

## Slide 17
Chart: 
| 0.5 | 1 | 2 | 3
a | 96.282 | 93.472 | 79.427 | 64.875
Ethylene
Area %
MPa
Chart: 
| 0.5 | 1 | 2 | 3
c | 0.35 | 1.288 | 7.27 | 13.252
g | 0.176 | 0.704 | 5.162 | 8.487
h | 0.283 | 0.584 | 2.162 | 2.866
Area %
Acetaldehyde
Ethanol
Diethylether
MPa
Diethylether
Acetaldehyde
Ethanol
Chart: 
| 0.1 | 0.2 | 0.4 | 0.6
 | 99.522 | 99.442 | 98.322 | 94.19
Chart: 
| 0.6 | 0.4 | 0.2 | 0.1
c | 1.6736 | 0.4619 | 0.189 | 0.069
g | 0.66824 | 0.287 | 0.115 | 0.087
h | 0.31 | 0.21 | 0.07 | 0.03
Ethylene
Area %
Area %
MPa
MPa
Standard flow configuration
High pressure flow configuration
Effect of pressure on the catalytic conversion of ethylene

## Slide 18
SUMMARY
● Tandem µ-Reactor facilitates the rapid characterization of catalysts
● Full spectrum of operating parameters can be investigated – automatically
● Real time analysis of gaseous or liquid samples
● automated analysis of solids
● species identification using MS
The development of new catalysts means new products, lower costs, and a broader range of feedstocks

## Slide 20
Design of Tandem µ-Reactor
20
GC Injector
1st µ-Reactor
(40 - 900ºC,
Max. 200 ºC/min)
2nd µ-Reactor
(40 - 900ºC,
max: 200 ºC/min)
Carrier gas
Reactant
gas
（Three gas
selection）
SS tube
Catalysis bed
Quartz wool
6 mm o.d.
( 5 mm i.d.)
O-ring (Viton)
4 mm o.d.
( 2 and 3 mm i.d.)
Quartz Catalyst tube
Inert stainless steel tube
40
Spring B

## Slide 21
Sample cup
Carousel
“Tandem µ-Reactor” with Auto-shot sampler solid/viscous liquid sample
GC
MS
Tandem
µ-Reactor
Auto-Shot
Sampler
Operation under carrier gas pressure is below 0.04 MPa

## Slide 22
Rapid catalyst screening using a high pressure, tandem micro-reactor GC/MS
R.R. Freeman(1), Chu Watanabe(1), Young-Min Kim(1), Prof. Norio Teramae(2)