## Slide 1: Efficient Cubane Catalysts for Artificial Water Splitting
Sandra Luber
September 14th, 2015

## Slide 2: Nature: water splitting for carbohydrates & oxygen
Chemistry: 2H2O → 2H2 + O2

## Slide 3: Nature’s photosystem II
Y. Umena, , K. Kawakami, J.-R. Shen, N. Kamiya, Nature 2011 (473) 55.

## Slide 4: Oxygen evolving complex (OEC)
Y. Umena, K. Kawakami, J.-R. Shen, N. Kamiya, Nature 2011 (473) 55.
K. N. Ferreira, T. M. Iverson, K. Maghlaoui, J. Barber, S. Iwata, Science 2006 (303) 1838.
2H2O → 4 H+ + 4 e- + O2

## Slide 5: Does the crystal structure belong to the catalytic ground state?
EXAFS and DFT calculations:
New X-ray structure suffers
from oxidation damage
S. Luber, I. Rivalta, Y. Umena, K. Kawakami, J.-R. Shen, N. Kamiya, G. W. Brudvig, V. S. Batista, Biochemistry 2011 (50) 6308.

## Slide 6: S1-state model via DFT QM/MM
S. Luber, I. Rivalta, Y. Umena, K. Kawakami, J.-R. Shen, N. Kamiya, G. W. Brudvig, V. S. Batista, Biochemistry 2011 (50) 6308.
Dark blue:
XRD model
Model in agreement with
(anisotropic) EXAFS data

## Slide 7: Artificial photosynthesis at University of Zurich
University Research Priority Program: Light to Chemical Energy Conversion (LightChEC)
www.welldays.ch
Oxygen: challenging half reaction
Hydrogen: lightweight fuel
www.zeit.de
H2O
www.aerzteblatt.de

## Slide 8: The LightChEC Strategy
H2O
O2
-
-
-
-
-
-
H2O
H2
Cat 2
Cat 1
Light transfer
Electronic chain
Efficiency
LINK?
Water Oxidation Catalysts (WOCs) = bottleneck
Robust WOCs with abundant metals (Co, Mn)
Mimicking millions of years of evolution with molecules?

## Slide 9: PSII mimics
OUR MISSION: Active Co-cubane
closer to PSII
Magic cube
E. Y. Tsui, R. Tran, J. Yano, T. Agapie, Nat. Chem. 2013 (5) 293
Mn PSII mimics: No WOC activity
Only Co-cubane: [CoIII4O4(OAc)4(py)4]
+ derivatives
N. S. McCool, D. M. Robinson, J. E. Sheats, G. C. Dismukes, J. Am. Chem. Soc. 2011 (133) 11446 M. Bonchio et al., J. Am. Chem. Soc. 2012 (134) 11104
BUT: WOC activity results
from CoII impurities
A. M. Ullman, Y. Liu, M. Huynh, D. K. Bediako, H. Wang, B. L. Anderson, D. C. Powers, J. J. Breen, H. D. Abruna, D. C. Nocera, J. Am. Chem. Soc. 2014 (136) 17681

## Slide 10: New Co(II)-cubane WOC
[CoII4(hmp)4(μ-OAc)2(μ2-OAc)2(H2O)2]
hmp = 2-(hyxdroxymethyl)pyridine
First cubane with Co(II) metal centers
F. Evangelisti, R. Güttinger, R. Moré, S. Luber, G. R. Patzke, J. Am. Chem. Soc. 2013 (135) 18734 & CHIMIA 2014 Highlight
Collaboration with G. R. Patzke (UZH)

## Slide 11: {CoII4O4} Cubane: Stability
Solid state EXAFS spectrum: agrees with crystal structure
DFT calculations: HS Co(II), S = 6 ground state
Solution EXAFS: {Co4O4} core intact
Radical coupling mechanism as for HS Mn centers in OEC?

## Slide 12: Closer to OEC: mimic redox-inert metal center
F. Evangelisti, R. Güttinger, R. Moré, S. Luber, G. R. Patzke, J. Am. Chem. Soc., 2013 (135) 18734.
F. Evangelisti, R. Moré, F. Hodel, S. Luber, G. R. Patzke, J. Am. Chem. Soc., 2015 (137) 11076.
{Co3LnO4}
{Mn4CaO5}
{Co4O4}
OEC
Ln = Er, Ho, Yb, Tm

## Slide 14: What is the catalytic ground state of {Co4O4}?
F
ΔE [kcal/mol] | 
COSMO solvent continuum model | -30.7
COSMO + 45 H2O | 8.7
68 H2O (QM) + 260 H2O (MM) | 14.9
1st solvation shell (68 H2O) | 5.4
1st solvation shell 2 | 11.6
1st solvation shell 3 | 10.9
DFT-based molecular dynamics (328 H2O) | 30.0
F. Hodel, J. Hutter, S. Luber, to be submitted.
Detailed reaction path further investigated
via minimum energy path calculations
and metadynamics

## Slide 15: Partial detachment of acetate ligand – {Co3ErO4}
System | ΔE [kcal/mol]
a | -50
b | -75
DFT-based molecular dynamics

## Slide 16: Influence of buffer molecules
System | ΔE [kcal/mol]
a | 31
b | 38
c | 44
d | -6
F. Evangelisti, R. Moré, F. Hodel, S. Luber, G. R. Patzke, J. Am. Chem. Soc., 2015 (137) 11076.
DFT-based
molecular dynamics

## Slide 17: What is the oxidation mechanism? Oxo-oxo coupling?

## Slide 18: Alternative: single site water attack

## Slide 19: Free energy profiles: single center vs. oxo-oxo coupling
F. Hodel, J. Hutter, S. Luber, to be submitted.

## Slide 20
Oxo-oxo coupling

## Slide 21: Energy profile: oxo-oxo coupling
Chart: image
 | 0 | 41.228 | 39.2055 | 22.5244 | 12.7598 | 36.0724 | 45.074 | 32.3192

## Slide 22
Chart: image
 | 0 | 41.228 | 39.2055 | 22.5244 | 12.7598 | 36.0724 | 45.074 | 32.3192

## Slide 23
Chart: image
 | 0 | 41.228 | 39.2055 | 22.5244 | 12.7598 | 36.0724 | 45.074 | 32.3192

## Slide 24
Chart: image
 | 0 | 41.228 | 39.2055 | 22.5244 | 12.7598 | 36.0724 | 45.074 | 32.3192

## Slide 25
Chart: image
 | 0 | 41.228 | 39.2055 | 22.5244 | 12.7598 | 36.0724 | 45.074 | 32.3192

## Slide 26
Chart: image
 | 0 | 41.228 | 39.2055 | 22.5244 | 12.7598 | 36.0724 | 45.074 | 32.3192

## Slide 27
Chart: image
 | 0 | 41.228 | 39.2055 | 22.5244 | 12.7598 | 36.0724 | 45.074 | 32.3192

## Slide 28
Chart: image
 | 0 | 41.228 | 39.2055 | 22.5244 | 12.7598 | 36.0724 | 45.074 | 32.3192

## Slide 29: Summary
Artificial water splitting: promising route for sustainable hydrogen production (LightChEC program, UZH)
Cubanes as mimics for the oxygen-evolving center of nature’s photosystem II
{CoII4O4} cubanes: stable water oxidation catalysts
F. Evangelisti, R. Güttinger, R. Moré, S. Luber, G. R. Patzke, J. Am. Chem. Soc., 2013 (135) 18734
{CoII3LnO4}: more efficient and excellent model systems for investigation of nuclearity and influence of redox-inert cations
-> higher ligand flexibility
F. Evangelisti, R. Moré, F. Hodel, S. Luber, G. R. Patzke, J. Am. Chem. Soc., 2015 (137) 11076
In depth study of ligand-exchange reactions via both static and dynamic computational methods
Pioneering calculations of water oxidation mechanisms
F. Hodel, J. Hutter, S. Luber, to be submitted.

## Slide 30: Acknowledgement
Fabio Evangelisti, René Moré, Greta R. Patzke (UZH)
Florian Hodel, Mauro Schilling (UZH)
Jürg Hutter (UZH)
Funding: UZH, National Center of Competence in Research MARVEL (Materials’ Revolution)
Swiss national supercomputing center (project s502)

## Slide 31: Metadynamics: replacement of monodentate acetate by hydroxide